[DEPARTMENT] Concrete

[CATEGORY] Fresh and Hardened Concrete Testing

[CATEGORY] Sampling, Consistency and Workability
The correct sampling and mixing of fresh concrete is important if test results are to be reliable. Most of the equipment necessary for efficient sampling and mixing is standard laboratory equipment detailed in the Laboratory Equipment section.To ensure that concrete achieves its maximum possible strength and yet retains its ease of placing on site, it is essential that the design of the concrete mix, in relation to the water-cement ratio and workability, is closely controlled.

[PRODUCT GROUP] Slump Test
*Test is appropriate for concrete mixes of medium and high workability.The test is carried out by filling the slump cone with freshly mixed concrete, which is tamped with a steel rod in three layers. The concrete is levelled off with the top of the slump cone, the cone removed, and the slump of the sample is immediately measured.

[PRODUCT] Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Steel, 600 mm long x 16 mm dia, hemispherical at both ends

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Tamping Rod
	
Weight, kg
	0.95 kg

_Related Products_
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150mm Aggregate Crushing Value Apparatus. Supplied Complete with Metal Measure and Tamping Rod. (42-4300)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
Main: Bulk Density Measure 30 Litre (34-2800)
Main: Slump Cone (34-0110)
Main: Vibro Consistometer (34-0300/01)

[PRODUCT] 300 mm Stainless Steel Rule. (34-0140)

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Steel Rule
	
Weight, kg
	0.06 kg

_Related Products_
Main: Slump Cone (34-0110)

[PRODUCT] Base Plate for Slump Test. (34-0160)

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Base Plate
	
Weight, kg
	2 kg

_Related Products_
Main: Slump Cone (34-0110)

[PRODUCT] Slump Test Set BS & ASTM. C/W Slump Cone Base Plate Steel Rule Tamping Rod & Funnel. (34-0192)
BS and ASTM comprising of slump cone, base plate, steel rule, tamping rod and funnel.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Slump Test Set
	
Weight, kg
	6.87 kg

_Related Products_
Accessory: Sample Tray - 1200 x 1160 x 50 mm (81-4230)
Accessory: Shovel - With flat blade (81-0240)
Accessory: Stopwatch (81-0521)

[PRODUCT] Aluminium Scoop Large (81-0220)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Large Aluminium Scoop
	
Weight, kg
	0.294 kg

_Related Products_
Main: 100 X 100 X 500mm Beam Mould. (34-5003)
Main: 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
Main: 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150 X 150 X 750mm Beam Mould. (34-5053)
Main: 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
Main: 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)
Main: Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
Main: Apparatus for Determining Flow In Concrete (Flow Table). (34-0450)
Main: Bulk Density Measure 10 Litre (34-2830)
Main: Slump Cone (34-0110)
Main: Vibro Consistometer (34-0300/01)

[PRODUCT] Slump Cone (34-0110)
Complies with EN 12350-2, ASTM C143 and AASHTO T119

_Standards_
ASTM C143, ASTM C192, AASHTO T23, AASHTO T119, ASTM T126

_Attributes_
Description
	Slump Cone
	
Weight, kg
	1.3 kg
	
Weight, lbs
	5.5

_Specification_
Construction
	Seamless, heavy-gauge spun steel; 0.45" (1.1 mm) min. Thickness.
	
Finish
	Plated for rust and corrosion resistance.
	
Dimensions
	100 mm top diam. X 200 mm bottom diam. (without foot pieces) x 300 mm h.
	
Weights
	Net 5.5 lbs (2.5kg)

_Related Products_
Accessory: 300 mm Stainless Steel Rule. (34-0140)
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Base Plate for Slump Test. (34-0160)
Accessory: Cement Pan (34-0152)
Accessory: Graduated Tamping Rod (34-0132)
Main: Metal Slump Cone - English (34-0108)
Accessory: Sample Tray - 1200 x 1160 x 50 mm (81-4230)
Accessory: Shovel - With flat blade (81-0240)
Accessory: Slump Cone Base (34-0150)
Accessory: Slump Cone Funnel (34-0180)
Accessory: Stopwatch (81-0521)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)

[PRODUCT] Slump Cone Funnel (34-0180)

_Standards_
ASTM C143, ASTM C192, AASHTO T23, AASHTO T119, ASTM T126

_Attributes_
Description
	Slump Cone Funnel
	
Weight, kg
	1.3 kg
	
Base Dimensions l x w x h, ”
	208.59

_Related Products_
Main: Metal Slump Cone - English (34-0108)
Main: Portable Slump Test Set (EL3010E)
Main: Slump Cone (34-0110)
Accessory: Slump Cone Base (34-0150)
Main: Slump Test Set (EL3020E)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] K-Slump Tester
* Simple and economical to use.* Reduces testing time.* No special calibration required.* Plated for rust resistance and long life..The K-Slump Tester was developed to determine the slump and workability of fresh concrete. The device can be used for in-place measurements and for measurements inside of test molds and forms. The device is used as an indicator to correlate to the standard slump test.In operation, the K-Slump Tester is wetted and inserted into the concrete for 40 seconds. The K-Slump reading is then taken on the scale to the height that the concrete has penetrated the tester. The tester is then removed from the concrete vertically and the workability reading is taken on the scale as the height of concrete retained in the tester. After the readings, the unit is easily cleaned with water.

[PRODUCT] K-slump Tester (34-0580)
Developed to determine the workability of fresh concrete and the degree of concrete compaction placed in formwork. The apparatus can be used for in-place measurements of concrete in test moulds and forms and may be correlated to the standard slump test. It is simple, economical to use and reduces testing time. No special calibration is required.

_Attributes_
Description
	K-Slump Tester
	
Test Time, secs
	60
	
Weight, kg
	450 g

_Specification_
Construction
	Nickel Plated Steel. Calibrated 3/4" (19 mm) diam. Hollow tube; pointed insertion end; round disc controls depth of penetration.
	
Openings
	Two groups through which concrete enters.
	
Test time
	60 seconds
	
Weight
	Net 1 lb (445 g)

_Related Products_
Main: Portable Slump Test Set (EL3010E)
Main: Slump Test Set (EL3020E)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Weight, kg
	N/A for this Product Group

[PRODUCT GROUP] Vebe Time
*Test appropriate for concrete mixes of low and very low workabilityThis method is a mechanised variation of the slump test and includes a determination of the workability of concrete. It is based on the principle of subjecting the concrete to vibration after removal of the slump cone.The assembly is mounted upon a small vibrating table operating at a fixed amplitude and frequency. The time to complete the required vibration gives an indication of the concrete workability.Special Note: The consistometer must be operated from an electrical supply of 50 Hz in order to comply with the fixed test frequency specified.

[PRODUCT] Vibro Consistometer (34-0300/01)
Comprising of vibrating table, container, slump cone, graduated rod and plate. For 220 - 240 V AC, 50 Hz, 1 ph.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Voltage Supply
	220 - 240 V AC, 50 Hz, 1 ph
	
Description
	Vibro Consistometer

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Sample Tray - 1200 x 1160 x 50 mm (81-4230)
Accessory: Shovel - With flat blade (81-0240)
Accessory: Stopwatch (81-0521)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Voltage
	N/A for this Product Group

[PRODUCT GROUP] Flow Table
 	* Test appropriate for concrete mixes of high and very high workability.This test will be of interest to those involved with concrete having a high workability. The test determines the flow index as an arithmetic mean of the diameter of the specimen after working on a flow table. The apparatus consists of a mould, flow table, wooden tamper, metre rule and a float.

[PRODUCT] Apparatus for Determining Flow In Concrete (Flow Table). (34-0450)
Comprising of mould, flow, tamper, metre rule, float and stopwatch

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Flow Table

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Sample Tray - 1200 x 1160 x 50 mm (81-4230)
Accessory: Shovel - With flat blade (81-0240)
Accessory: Stopwatch (81-0521)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Setting Time by Penetration Resistance
This method covers the determination of setting time of the mortar fraction of concrete mixes and is only suitable on mortars with slump values greater than zero. The definition of the initial and final setting time is taken as the period from when water was first added to the mix until the measured penetration resistance is 500 lbf/in² and 4000 lbf/in² respectively.

[PRODUCT] Proctor Penetrometer Spring Type with Adaptor Stem.Supplied Complete with Set of Needle Points (29-3925)
Supplied without needle points

_Standards_
ASTM D1558

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Proctor Penetrometer - complete with set of needle points
	
Weight, kg
	2

_Related Products_
Accessory: Case for Proctor Penetrometer. (29-3933)
Accessory: Set of Needle Points 1 1/2 1/4 1/10 1/20 1/40 Inch Sq. (34-0810)
Accessory: Syringe with Rubber Bulb. (82-2820)

[PRODUCT] Set of Needle Points 1 1/2 1/4 1/10 1/20 1/40 Inch Sq. (34-0810)
Stainless steel, 1, 1/2, 1/4, /10, 1/20 and 1/40 in2 area (645, 323, 161, 65, 32 and 16 mm2) with stainless steel adaptor for the smaller needles.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Set of needle points

_Related Products_
Main: Proctor Penetrometer Spring Type with Adaptor Stem.Supplied Complete with Set of Needle Points (29-3925)

[PRODUCT] Syringe with Rubber Bulb. (82-2820)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Syringe with rubber bulb
	
Weight, kg
	0.5

_Related Products_
Main: Proctor Penetrometer Spring Type with Adaptor Stem.Supplied Complete with Set of Needle Points (29-3925)

[PRODUCT] Pocket Concrete Penetrometer (38-2695)
Supplied complete with belt-loop, canvas carrying case.

_Standards_
ASTM C187, ASTM C191, ASTM C780

_Attributes_
Description
	Pocket Concrete Penetrometer
	
Dimensions, diam. X length, ”
	3/4” (19 mm) diam. x 7” (178 mm) long.

_Specification_
Dimensions
	19 x 178 mm (diameter x length)
	
Shaft Needle
	Steel, 1/20 inÂ² surface area
	
Range
	0 to 700 lbf/inÂ²
	
Scale
	Direct-reading, indicator sleeve holds reading until released
	
Weight
	227 g
	
Needle
	Steel shaft; 1/20 sq. in. surface area.
	
Range
	0 to 700 psi.
	
Scale
	Direct-reading; indicator sleeve holds reading until released.
	
Dimensions
	3/4â€ (19 mm) diam. x 7â€ (178 mm) long.
	
Carrying Case
	Canvas, with belt-loop.
	
Weight
	Net 8 oz. (227 g).

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Air Entrainment
The determination of air content of freshly made concrete is detailed in EN 123450 and ASTM C236, where the importance of two main applications is highlighted. The primary purpose of entraining air in concrete is to give the required resistance to weathering. The use of chemical additives to increase the workability of concrete often requires an air content check to be made.

[PRODUCT GROUP] Precision Air Entrainment Meter
The proper control of entrained air in concrete is recognized as one of the most important functions in modern concrete manufacture. For the concrete engineer, the ELE Precision Air Entrainment Meter offers an instrument for the testing and designing of concrete mixes.

[PRODUCT] Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Steel, 600 mm long x 16 mm dia, hemispherical at both ends

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Tamping Rod
	
Weight, kg
	0.95 kg

_Related Products_
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150mm Aggregate Crushing Value Apparatus. Supplied Complete with Metal Measure and Tamping Rod. (42-4300)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
Main: Bulk Density Measure 30 Litre (34-2800)
Main: Slump Cone (34-0110)
Main: Vibro Consistometer (34-0300/01)

[PRODUCT] Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
* 7 litre capacity* Shock-proof pressure gauge mounting* Lightweight aluminum construction* Heavy-duty plastic carrying case for easy transport to siteThe proper control of entrained air in concrete is recognized as one of the most important functions in modern concrete manufacture. For the concrete engineer, the ELE Precision Air Entrainment Meter offers an instrument for the testing and designing of concrete mixes.The instrument is designed so that the operating parts form an integral unit. The container is rigid, thus providing an accurate device for the performance of unit weight testing. For convenience, the tare weight in grams is stamped on the bottom. When used with the supplied nomograph, the air meter provides quick and easy particle density and percent of free moisture in aggregate determinations.

_Standards_
ASTM C231, AASHTO T152

_Attributes_
Description
	Air Entrainment Meter - B Type
	
External Dimensions dia x height, ”
	9.75 x 13.25

_Specification_
Dimensions
	248 x 345 mm (diameter x height)
	
Capacity
	7 litres
	
Readings
	Up to 22% entrained air
	
Accuracy
	± 0.25% full scale
	
Aggregate size
	50 mm maximum
	
Container
	With tare weight stamped onbottom; 2-piece clamping devicefor positive seal
	
Pressure gauge
	In shock-proof mounting
	
Weight
	8 kg
	
Capacity
	1/4 cu. Ft. (0.007 m³)
	
Readings
	Up to 22% entrained air
	
Accuracy
	1/4% full scale
	
Aggregate Size
	2" (50.8 mm) maximum
	
Container
	With tare weight stamped on bottom; 2-piece clamping device for positive seal.
	
Water
	4 oz required
	
Initial Pressure
	Approx. 10 strokes needed
	
Pressure Gauge
	In shock-proof mounting
	
Tamping Rod
	Aluminium; 24" (610 mm) long
	
Dimensions
	9-3/4" diam. X 13-1/4" h. (248 x 337 mm)
	
Weight
	Net 15 lbs (6.8 kg)

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Spare/Consumable: Concrete Air Indicator (38-3280/10)
Main: Concrete Air Indicator Kit (34-3280)
Accessory: Float - Plasterer’s type (81-0340)
Spare/Consumable: Gauge Kit (34-3265/12)
Accessory: Graduated Tamping Rod (34-0132)
Main: Press-Ur-Meter Type A (34-3267)
Spare/Consumable: Pump Assembly (34-3265/10)
Accessory: Sample Tray - 1200 x 1160 x 50 mm (81-4230)
Accessory: Shovel - With flat blade (81-0240)
Main: Soft Headed Mallet. (29-5020)
Accessory: Stopwatch (81-0521)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Main: Volumetair (34-3272)

[PRODUCT] Compacting Bar 25mm Sq X 380mm (34-2910)
Steel, 380 x 25 mm (length x square) tamping area, EN/BS.

_Attributes_
Description
	Compacting bar

_Related Products_
Main: 100 X 100 X 500mm Beam Mould. (34-5003)
Main: 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
Main: 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150 X 150 X 750mm Beam Mould. (34-5053)
Main: 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
Main: 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)
Main: Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
Main: Apparatus for Determining Flow In Concrete (Flow Table). (34-0450)
Main: Bulk Density Measure 10 Litre (34-2830)
Main: Bulk Density Measure 30 Litre (34-2800)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Mixing Equipment
The efficient mixing of concrete prior to moulding specimens in the laboratory for subsequent testing is essential if quality specimens are to be manufactured. The object of mixing is to coat the surface of all aggregate particles with cement paste, and bring the mix to a uniform condition. Pan or rotating drum mixers are suitable for the mixing of small quantities of concrete, which are generally used in a laboratory.

[PRODUCT GROUP] ELE Concrete Mixer

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	
34-3540/01
	220 - 240 V 50 Hz
	
34-3540/06
	220 - 240 V 60 Hz

[PRODUCT GROUP] Tilting Drum Mixer

[PRODUCT] Tilting Drum Concrete Mixer 120/90L/ (4/3Cu.Ft) Complete with Stand (34-3590/01)
120/90 litre mixing capacity. For 220 - 240 V AC, 50 Hz, 1 ph.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Voltage Supply
	220 - 240 V AC, 50 Hz, 1 ph

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	N/A for this Product Group

[CATEGORY] Moulding Equipment
Test procedures require that specimens are cast in a number of standard sizes convenient for compressive and flexural strength determination. The engineering tolerances specified for moulds are very stringent and the internal finish of the surface must be of a high order to comply with the recommendations laid down in many International Standards. Moulds must not deform during manufacture of concrete specimens if the specimen dimensions are to be maintained.

[PRODUCT GROUP] Cube Moulds
These cube moulds are designed to produce accurate specimens while avoiding distortion over the length of the mould.

[PRODUCT] 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
2-part with clamp attached base plate.

_Attributes_
Cube mould type
	2 part
	
Specimen Size
	100 x 100 mm

_Specification_
Construction
	Bolted sides and clamped base plate
	
Finish
	Painted
	
Weight
	42 lb (19.1 kg)

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
2-part with clamp attached base plate.

_Attributes_
Cube mould type
	2 part
	
Specimen Size
	150 x 150 mm

_Specification_
Construction
	Bolted sides and clamped base plate
	
Finish
	Painted
	
Weight
	42 lb (19.1 kg)

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
4-part with clamp attached base plate.

_Attributes_
Cube mould type
	4 part
	
Specimen Size
	100 x 100 mm
	
Internal Dimensions dia x h, ”
	100 x 100 x 100

_Specification_
Construction
	Bolted sides and clamped base plate
	
Finish
	Painted
	
Weight
	20 lb (9.1 kg)

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
4-part with clamp attached base plate.

_Attributes_
Specimen Size
	150 x 150 mm
	
Cube mould type
	4 part
	
Internal Dimensions dia x h, ”
	150 x 150 x 150

_Specification_
Construction
	Bolted sides and clamped base plate
	
Finish
	Painted
	
Weight
	42 lb (19.1 kg)

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)
4-part with clamp attached base plate.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Cube mould type
	4 part
	
Specimen Size
	200 x 200 mm
	
Weight, kg
	35

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[GROUPED PRODUCT MATRIX]
Model No.
	Mould Type
	Specimen Size
	N/A for this Product Group

[PRODUCT GROUP] Cylinder Moulds
These cylinder moulds are designed to produce accurate specimens while avoiding distortion over the length of the mould.

[PRODUCT] 100mm Dia Cylinder Mould 200mm Long. (34-5210)
100 mm diameter x 200 mm long, complete with base plate.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Specimen Size
	100 x 200 mm
	
Weight, kg
	16

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 150mm Dia Cylinder Mould 150mm Long. (34-5230)
150 mm diameter x 150 mm long, complete with base plate.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Specimen Size
	150 x 150 mm
	
Weight, kg
	14

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 150mm Dia Cylinder Mould 300mm Long. (34-5260)
150 mm diameter x 300 mm long, complete with base plate and locking ring.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Specimen Size
	150 x 300 mm
	
Weight, kg
	12

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[GROUPED PRODUCT MATRIX]
Model No.
	Specimen Size
	N/A for this Product Group

[PRODUCT GROUP] Beam Moulds
These beam moulds are designed to produce accurate specimens while avoiding distortion over the length of the mould.

[PRODUCT] 100 X 100 X 500mm Beam Mould. (34-5003)
Complete with base plate

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Specimen Size
	100 x 100 x 500 mm

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[PRODUCT] 150 X 150 X 750mm Beam Mould. (34-5053)
Complete with base plate

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Specimen Size
	150 x 150 x 750 mm

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Mould Oil (25 Litre Drum) (82-7341)
Main: Soft Headed Mallet. (29-5020)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Accessory: Wire Brush (81-0705)

[GROUPED PRODUCT MATRIX]
Model No.
	Specimen Size
	N/A for this Product Group

[PRODUCT GROUP] Accessories for Concrete Moulds

[PRODUCT] Compacting Bar 25mm Sq X 380mm (34-2910)
Steel, 380 x 25 mm (length x square) tamping area, EN/BS.

_Attributes_
Description
	Compacting bar

_Related Products_
Main: 100 X 100 X 500mm Beam Mould. (34-5003)
Main: 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
Main: 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150 X 150 X 750mm Beam Mould. (34-5053)
Main: 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
Main: 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)
Main: Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
Main: Apparatus for Determining Flow In Concrete (Flow Table). (34-0450)
Main: Bulk Density Measure 10 Litre (34-2830)
Main: Bulk Density Measure 30 Litre (34-2800)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)

[PRODUCT] Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)
Steel, 600 mm long x 16 mm dia, hemispherical at both ends

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Tamping Rod
	
Weight, kg
	0.95 kg

_Related Products_
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150mm Aggregate Crushing Value Apparatus. Supplied Complete with Metal Measure and Tamping Rod. (42-4300)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: Air Entrainment Meter B Type Complete with Carrying Case. Supplied with Aluminium Tamping Bar. (34-3265)
Main: Bulk Density Measure 30 Litre (34-2800)
Main: Slump Cone (34-0110)
Main: Vibro Consistometer (34-0300/01)

[PRODUCT] Wire Brush (81-0705)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Wire Brush
	
Weight, kg
	0.3

_Related Products_
Main: 100 X 100 X 500mm Beam Mould. (34-5003)
Main: 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
Main: 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150 X 150 X 750mm Beam Mould. (34-5053)
Main: 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
Main: 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)
Main: Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)

[PRODUCT] Mould Oil (25 Litre Drum) (82-7341)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Mould Oil
	
Capacity, litres
	25 litre

_Related Products_
Main: 100 X 100 X 500mm Beam Mould. (34-5003)
Main: 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
Main: 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150 X 150 X 750mm Beam Mould. (34-5053)
Main: 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
Main: 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Compaction
The strength, durability and finish of concrete rely in part on the adequate compaction of the mix. An increasing number of contract specifications call for various forms of vibro-compacted concrete as a means to achieve a better and more consistent mixture. It should however be remembered that fluid mixes may segregate when vibrated in which case it may be more appropriate to compact using a tamping bar or rod during laboratory mix design.

[PRODUCT GROUP] Vibrating Poker

[PRODUCT] Vibrating Poker 25mm Dia Tip 290mm Long. 220-240V 50/60Hz 1Ph. (34-6431/01)
* High amplitude and speed* Flexible shaft for long lifeUsed as an internal means of vibratory compaction. The poker is inserted into the concrete which is then compacted by the high frequency vibration action. For use in either laboratory or site environments, the diameter of the vibrating tip must not exceed 25% of the smallest dimension of the specimen.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220 - 240 V AC, 50 - 60 Hz, 1 ph

_Attributes_
Voltage Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Specification_
Tip Dimensions
	22 mm diamenter x 250 mm long
	
Shaft dimensions
	2.0 m long
	
Speed
	12,000 vibrations/min.
	
Overall Dimensions
	200 x 300 x 350 mm
	
Weight
	7 kg

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	N/A for this Product Group

[PRODUCT GROUP] Vibrating Table

[PRODUCT] Vibrating Table 600 X 400mm Table Top. 220-240V 50Hz 1Ph.. Supplied with clamping assm. (34-6250/01)
Vibrating table mounted on a steel stand, supplied with clamp assembly.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** 3000 cycles per minute. For 220 - 240 V AC, 50 Hz, 1 ph.

_Attributes_
Voltage Supply
	220 - 240 V AC, 50 Hz, 1 ph

_Specification_
Dimensions (table top)
	600 x 400 mm
	
Maximum no. Cube moulds
	2 x 150 mm²
	
Clamp Assembly
	Single
	
Weight
	60 kg

_Related Products_
Main: 100 X 100 X 500mm Beam Mould. (34-5003)
Main: 100mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4650)
Main: 100mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4520)
Main: 100mm Dia Cylinder Mould 200mm Long. (34-5210)
Main: 150 X 150 X 750mm Beam Mould. (34-5053)
Main: 150mm Cube Mould 2-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4670)
Main: 150mm Cube Mould 4-Part Clamp Type. Cast Iron Construction. BS EN Compliant. (34-4570)
Main: 150mm Dia Cylinder Mould 150mm Long. (34-5230)
Main: 150mm Dia Cylinder Mould 300mm Long. (34-5260)
Main: 200mm Cube Mould Clamp Type. Cast Iron Construction. Stamped Mould Sections. EN Compliant. (34-4620)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Wire Brush (81-0705)

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	N/A for this Product Group

[CATEGORY] Curing of Specimens
The correct environment for curing concrete test specimens is important to achieve consistent and reproducible test results. Two primary factors must be taken into consideration to satisfy the requirements, namely to maintain a stable temperature and to prevent loss of moisture from the specimen. A standard curing temperature of 20ºC is usually specified and should be maintained at the required degree of accuracy. The use of water to prevent loss of moisture is the method most commonly used. In tropical climates a curing temperature of 25ºC is often acceptable.

[PRODUCT GROUP] Large Curing Tank

[PRODUCT] Large Curing Tank C/W with Circulating Pump Heater/Thermostat Unit and Lower Rack (34-6575/01)
This curing tank is supplied complete with a submersible pump, immersion heater/thermostat unit and separate control panel. The tank includes a lower rack as standard and is designed to maintain the temperature at 20 ± 2ºC, providing that the ambient temperature does not fall below 15ºC or rise above 20ºC.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** Supplied as specified. For 220 - 240 V AC, 50 - 60 Hz, 1 ph.

_Attributes_
Description
	Curing/soaking tank

_Specification_
Internal Dimensions
	1040 x 1040 x 605 mm (l x w x h)
	
Capacity
	650 litres
	
Rated Power
	2000 watt
	
Weight
	60 kg

_Related Products_
Main: Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)
Accessory: Maximum and Minimum Thermometer (82-5310)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Capping of Cylinders
When conducting a compressive strength test on a concrete cylinder it is important that the ends of the specimen are flat and parallel to each other. The trowelled face of a prepared concrete cylinder, or both ends of a concrete core, will require treatment to obtain these conditions.

[PRODUCT GROUP] Melting Pot
This unit is suitable for melting wax and capping compound and comprises a metal container in a welllagged steel jacket. A thermostatic control and stand-by heat switch are fitted. Supplied complete with lift-off cover.

[PRODUCT] Melting Pot 4 Litre Capacity. 50 to 300 Deg. C. Temperature Range. (34-6122/01)
This unit is suitable for melting wax and capping compound and comprises a metal container in a welllagged steel jacket. A thermostatic control and stand-by heat switch are fitted. Supplied complete with lift-off cover.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** for 220 - 240 V AC, 50 - 60 Hz, 1 ph.

_Attributes_
Voltage Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Specification_
Internal Dimensions (diameter x depth
	140 x 150 mm
	
External Dimensions (diameter x depth)
	250 x 165 mm
	
Capacity
	4 litres
	
Rated Power
	300 watt
	
Temperature range
	50 to 300ºC
	
Weight
	7 kg
	
Internal Dimensions (diameter x depth
	140 x 150 mm
	
External Dimensions (diameter x depth)
	250 x 165 mm
	
Capacity
	4 litres
	
Rated Power
	300 watt
	
Temperature range
	50 to 300ºC
	
Weight
	7 kg

_Related Products_
Main: Cylinder Capping Frame Complete with 100mm and 150mm Dia Capping Plates. (34-6031)
Main: Flake Capping Compound to ASTM C617 22Kg (34-6100)
Accessory: Vibrating Hammer (47-0455/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	N/A for this Product Group

[PRODUCT GROUP] Sulphur Compound Method
The sulphur compound method is a hot process and offers a considerable saving in time and labour over the mortar capping method. The method is virtually instant and the compound can often be recovered for further use.Warning: The sulphur compound, when hot, will give off sulphur fumes, and therefore it is important that good ventilation, or preferably a fume cupboard, is available in the laboratory.The sulphur compound method is a hot process and offers a considerable saving in time and labour over the mortar capping method. The method is virtually instant and the compound can often be recovered for further use.

[PRODUCT] Flake Capping Compound to ASTM C617 22Kg (34-6100)
Supplied in 22 kg box.

_Standards_
ASTM C617, AASHTO T231

_Attributes_
Description
	Flake Capping Compound
	
Melting Range, °F
	230-240

_Specification_
Density
	13 7 lbs./cu. ft. (2,186 kg/cu. m.).
	
Tensile Strength
	605 psi (4.2 x 105 kg/sq m.) after 48 hrs.
	
Compressive Strength
	5,000 psi (3.6 x 106 kg/sq m.) minimum, after2 hrs.
	
Melting Range
	23 0Â°-24 0Â°F (11 0Â°-115 Â°C).
	
Optimum Pouring Range
	260Â°-290Â°F (12 6Â°-143 Â°C).
	
Weight
	Net 50 lbs. (22 .7 kg); Shpg. 52 lbs. (23 .6 kg).

_Related Products_
Main: 4" Compression Pads 60 Durometer (34-6132/10)
Main: 4" Compression Pads 70 Durometer (34-6132/12)
Main: 4" Retaining Caps (34-6132)
Main: 6" Compression Pads 60 Durometer (34-6134/10)
Main: 6" Compression Pads 70 Durometer (34-6134/12)
Accessory: 6" Retaining Caps (34-6134)
Main: Capping Compound Warming Pots 110vAC (34-6125/02)
Main: Capping Compound Warming Pots 220vAC (34-6125/01)
Main: Cylinder Capping Frame Complete with 100mm and 150mm Dia Capping Plates. (34-6031)
Main: Cylinder Capping Set (3000/01)
Main: Cylinder Capping Set (3000/02)
Main: Melting Pot 4 Litre Capacity. 50 to 300 Deg. C. Temperature Range. (34-6122/01)

[PRODUCT] Cylinder Capping Frame Complete with 100mm and 150mm Dia Capping Plates. (34-6031)
Comprising of a vertical support, mounted on a steel base designed to accommodate both sizes of capping plates. Supplied complete with 100 mm and 150 mm capping plates.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Cylinder Capping Frame
	
Weight, kg
	10

_Related Products_
Main: Flake Capping Compound to ASTM C617 22Kg (34-6100)
Main: Melting Pot 4 Litre Capacity. 50 to 300 Deg. C. Temperature Range. (34-6122/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Density of Fresh and Hardened Concrete
The density of both fresh and hardened concrete is of interest to the engineer for numerous reasons including its effect on durability, strength and resistance to permeability. Hardened concrete density is determined either by simple dimensional checks, followed by weighing and calculation, or by weight in air/water buoyancy methods.

[PRODUCT GROUP] Fresh Concrete - Bulk Density Measures

[PRODUCT] Bulk Density Measure 10 Litre (34-2830)
Manufactured from heavy gauge steel these bulk density measures comply with the requirements of either BS 812, EN 1097-3, 12350-6 or ASTM C138. All measures incorporate carrying handles as standard.

_Standards_
EN 12350-6

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For other bulk density measures see the aggregates section

_Attributes_
Capacity, litres
	10

_Related Products_
Accessory: Aluminium Scoop Large (81-0220)
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Float - Plasterer’s type (81-0340)
Accessory: Glass Plate. (24-0430)
Accessory: Sample Tray - 1200 x 1160 x 50 mm (81-4230)
Accessory: Shovel - With flat blade (81-0240)
Main: Soft Headed Mallet. (29-5020)
Accessory: Straight Edge 300mm. (24-9010)

[PRODUCT] Bulk Density Measure 15 Litre (34-2820)
Manufactured from heavy gauge steel these bulk density measures comply with the requirements of either BS 812, EN 1097-3, 12350-6 or ASTM C138. All measures incorporate carrying handles as standard.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For other bulk density measures see the aggregates section

_Attributes_
Capacity, litres
	15

[PRODUCT] Bulk Density Measure 30 Litre (34-2800)
Manufactured from heavy gauge steel these bulk density measures comply with the requirements of either BS 812, EN 1097-3, 12350-6 or ASTM C138. All measures incorporate carrying handles as standard.

_Standards_
BS 812, EN 1097-3, EN 12350-6, ASTM C138

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For other bulk density measures see the aggregates section

_Attributes_
Capacity, litres
	30

_Related Products_
Accessory: Compacting Bar 25mm Sq X 380mm (34-2910)
Accessory: Tamping Rod 16mm Dia X 600mm Long Hemispherical At Both Ends. (34-0130)

[GROUPED PRODUCT MATRIX]
Model No.
	Capacity, litres
	N/A for this Product Group

[PRODUCT GROUP] Hardened Concrete - Buoyancy Balance
The density of hardened concrete specimens such as cubes and cylinders can be quickly and accurately determined using a Buoyancy Balance.The buoyancy balance system developed by ELE consists of a rigid support frame, incorporating a water tank mounted on a platform. The water tank has internal dimensions of 380 x 240 x 280 mm (l x w x h).A mechanical lifting device is used to raise the water tank through the frame height immersing the specimen suspended below the balance. The balance supplied calculates the specific gravity of the sample automatically.The balance may also be used as a standard weighing device, thus providing a versatile and comprehensive weighing system in the laboratory.

[PRODUCT] Cradle (34-8105)

_Standards_
EN 12697-32, EN 13280-4, BS 598-104

_Attributes_
Description
	Cradle
	
Weight, lbs
	1.24

_Related Products_
Main: Buoyancy Balance (34-8100/09)
Main: ELE Buoyancy Balance (34-8100/02)
Accessory: Vibrating Hammer (47-0455/01)

[PRODUCT] Buoyancy Balance (34-8100/09)

_Standards_
EN 12697-32, EN 13280-4, BS 598-104

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Buoyancy Balance
	
Power Supply
	110 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Accessory: Cradle (34-8105)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Drying, Shrinkage and Moisture Movement
The apparatus has been designed and manufactured to the recommendations laid down in BS, EN and ASTM standards where tests are required on laboratory specimens, or on specimens taken from existing structures. The test procedure specifies a method for determining the change in length of a concrete or mortar sample brought about by a change in moisture content.

[PRODUCT GROUP] Measuring Equipment

[PRODUCT] Drying Shrinkage & Moisture Movement Apparatus Complete with Two Calibration Rods (34-8500)
Conforming to the requirements of EN 1367-4 and ASTM C490 comprising a steel frame with an adjustable-height beam and a dial gauge with 0.002 mm divisions. Supplied with two calibration rods EN and ASTM.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Drying Shrinkage & Moisture Movement Apparatus
	
Weight, kg
	4.5

_Related Products_
Spare/Consumable: Length Comparator 11 5/8in Total Length; 3/8in Dia Tips. (34-8505/10)

[PRODUCT] Length Comparator 11 5/8in Total Length; 3/8in Dia Tips. (34-8505/10)
115/8 inch total length.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Spare length comparator

_Related Products_
Main: Drying Shrinkage & Moisture Movement Apparatus Complete with Two Calibration Rods (34-8500)

[PRODUCT] Length Comparator (SP34-8501)
Used to measure the length variations of mortar specimens after autoclave soundness tests. The top beam is adjustable to suit the specimen's length. It also measures the linear shrinkage of specimens having different dimensions such as 40 x 40 x 160 mm or 25 x 25 x 250 mm. Supplied with Digital Gauge, 15.3 mm travel by 0.001 mm divisions complete with battery.

_Standards_
ASTM C348, ASTM C490, EN 12617-4, EN 12808-4

_Attributes_
Description
	Length Comparator

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Prism Moulds and Inserts

[PRODUCT] Two Gang Prism Mould Produces 1 Inch Square X 11 1/4 Inch Long Specimen (10 Inch Gauge Length) (34-8544)
To produce specimens 1 inch square x 11¼ inches long to ASTM C490. The mould is constructed so that the gauge length can be set within ± 0.1 inch limits.

_Standards_
ASTM C141, ASTM C151, ASTM C157, ASTM C227, ASTM C490, ASTM C531, AASHTO T107

_Attributes_
Description
	Two Gang Prism Mould 1" x 11 1/4"
	
Gauge Length
	10” (254 mm) between inner ends of embedded contact points.

_Specification_
Construction
	Plated steel.
	
Gauge Length
	10â€ (254 mm) between inner ends of embedded contact points.
	
Weight
	Net 20 lbs. (9.1 kg).

_Related Products_
Accessory: Contact Points (34-8548)
Accessory: Inserts for 34-8544 (Pack of 10) (34-8547)
Main: Single mould (34-8545)

[PRODUCT] Prism Mould 75 X 75 X 254mm (34-8538)
For producing specimens 75mm square x 254mm gauge length to BS 812-123. The mould is made of steel and constructed so that the gauge length can be set within ± 2.54 mm limits. The overall length of the manufactured prism with steel inserts is 292mm.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Prism Mould 75 x 75 x 254 mm
	
Weight, kg
	6.5

_Related Products_
Accessory: Steel Inserts for El34-8538 (Pack of 10) (34-8541)

[PRODUCT] Steel Inserts for El34-8538 (Pack of 10) (34-8541)
For use with prism mould 34-8538. Supplied in pack of 10.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Steel Inserts for prism mould 75 x 75 x 254 mm
	
Weight, kg
	0.5

_Related Products_
Main: Prism Mould 75 X 75 X 254mm (34-8538)

[PRODUCT] Inserts for 34-8544 (Pack of 10) (34-8547)
For use with prism mould 34-8544. Supplied in pack of 10.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Inserts for Prism Mould 1" x 11 1/4"
	
Weight, kg
	0.7

_Related Products_
Main: Two Gang Prism Mould Produces 1 Inch Square X 11 1/4 Inch Long Specimen (10 Inch Gauge Length) (34-8544)

[PRODUCT] Humidity Cabinet to En196 320 Litre Capacity (39-1300/01)
For 220 - 240 V AC, 50 Hz, 1 ph.

_Standards_
EN 196-1, EN 459-2, BS 3892-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** 10 Reinforced Shelves and Circular Chart Recorder

_Attributes_
Description
	Humidity Cabinet
	
Capacity, litres
	320
	
Voltage Supply
	220 - 240 V AC, 50 Hz, 1 ph
	
Power Supply
	220-240 V AC, 50 Hz, 1 ph

_Specification_
Capacity
	320 litres
	
Dimensions External, Internal
	660 x 635 x 1745 mm,490 x 510 x 1275 mm
	
Temperature Range
	+5.0°C to +60°C
	
Fluctuation (better than)
	± 0.2ºC
	
Variation (better than)
	± 0.5ºC
	
Recorder:Circular chart type,Temperature,Humidity
	7 day,0 – 50ºC,0 – 100% RH
	
Rated power
	850 Watt
	
Number of shelves
	10
	
Weight
	151 kg

_Related Products_
Main: Humidity Cabinet BS EN 150 Litre Capacity 50Hz (SP39-1400/01)
Main: Humidity Cabinet BS EN 150 Litre Capacity 60Hz (SP39-1400/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/06)
Spare/Consumable: Replacement Circular Charts (39-1300/10)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Non-Destructive Testing of Hardened Concrete

[PRODUCT GROUP] Crack Detection

[PRODUCT] Crack Detection Microscope Magnification X 40 Measuring Range of 4mm In 0.02mm Divisions (35-2505)
Specifically designed for measuring crack width in concrete, this high definition microscope operates via an adjustable light source provided by high power batteries.Supplied in a pocket sized carrying case.

_Attributes_
Description
	Crack Detection Microscope
	
Divisions
	0.02

_Specification_
Dimensions (l x w x h)
	40 x 90 x 150 mm (in case)
	
Magnification
	x 40
	
Measuring range
	4 mm, 0.02 mm divs
	
Weight
	550 g
	
Dimensions (l x w x h)
	40 x 90 x 150 mm (in case)
	
Magnification
	x 40
	
Measuring range
	4 mm, 0.02 mm divs
	
Weight
	550 g
	
Magnification
	X 35 .
	
Measuring Range
	4 mm.
	
Divisions
	0.02 mm.
	
Dimensions
	1.5â€ x 3.5â€ x 6â€ (40 x 90 x 15 0 mm) in case.
	
Weight
	Net 19.4 oz. (55 0 g).

_Related Products_
Main: Calibrated Crack Monitor (35-2510)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Permeability of Concrete

[PRODUCT] Gwt Permeability Kit 0-6 Bar Range Supplied In A Carrying Case. (35-4043)
The Water Permeability Test Kit is a portable unit capable of measuring in-situ permeability. It has a dual measuring range of 0 - 1.5 bar or 0 - 6 bar. Consisting of a sealed water reservoir and all necessary attachments, the unit is supplied complete in a carrying case. Dimensions 460 x 310 x 100 mm ( l x w x h).

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Gwt Permeability Kit
	
Weight, kg
	3

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Rebar Detection

[PRODUCT] Profoscope Rebar Detector and Covermeter (35-2025)
The Profoscope is a versatile, fully-integrated rebar detector and cover meter with a unique real-time rebar visualization allowing the user to see the location of the rebar beneath the concrete surface to a maximum depth of 180 mm. This is coupled with rebar-proximity indicators and optical and acoustical locating aids. Rebar diameter can also be estimated within the specified testing range. The Profoscope combines these unique features in a compact, light device that allows the user to operate this rebar detector with one hand making the task of locating rebars a simple and efficient process. In addition, Proceq's rebar detector convinces through its intuitive user interface making rebar detection easy. *NOT AVAILABLE FOR SALE IN THE USA*

_Further Information_
 	* A rebar detector with real-time visualization of the rebars beneath the instrument 	* Visual indication of rebars in close proximity 	* The Profoscope is a rebar detector with the ability to identify the mid-point between rebars as well as the orientation of rebars 	* Optical and acoustical indication of rebar location and minimum cover alert 	* This rebar detector offers neighboring bar correction 	* Regional settings (metric, imperial) 	* Cordless and single handed operation 	* Switchable display backlight for dark environments 	* A rebar detector with icon-based language independent menus 	* Start-up test kit allows user to familiarize him/herself with all functions in a comfortable environment, wasting no time on site

_Attributes_
Desc
	Profoscope Rebar Detector

_Specification_
Tehcnical Data
	Profoscope
	
Power Supply
	2 x 1.5 V AA Batteries
	
Voltage Range
	3.6 V to 1.8 V
	
Dimensions
	205 x 92 x 41 mm (8 x 3.6 x 1.6")
	
Temperature Range
	-10°C to 60°C (14°F to 140°F)
	
Humidity Range
	0 to 100% rH
	
Protection Range
	IP54

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Surface Hardness
Surface hardness is used to measure the resistance of concrete to impact or penetration. From the measurements it is possible to obtain an estimation of the concrete strength and quality.

[PRODUCT GROUP] Surface Hardness
The method is based on the principle that the rebound of an elastic mass depends on the hardness of the surface which it strikes. The test is fast and is unlikely to cause damage to the concrete.

[PRODUCT] Standard Concrete Test Hammer (35-1480)
The hammer is intended for testing the quality of concrete in finished structures such as buildings and bridges. Supplied complete with carrying case and carborundum stone, the hammer is suitable for testing concrete with compressive strengths of 10 to 70 N/mm2.

_Standards_
ASTM C805

_Attributes_
Description
	Standard Concrete Test Hammer
	
Accuracy, %
	15

_Specification_
Body
	Includes indicator scale, calibration curves.
	
Calibration Curves
	Rebound number vs. compressive strength.
	
Rubbing Stone
	Prepares test surface.
	
Accuracy
	Within 15 %.
	
Carrying Case
	Plastic.
	
Weight
	Net 3 lbs. (1.4 kg).

_Related Products_
Main: Concrete Test Hammer - English  (35-1475)
Spare/Consumable: Rubbing Stone (35-1475/10)
Accessory: Testing Anvil (35-1530)

[PRODUCT] Testing Anvil (35-1530)

_Standards_
ASTM C805

_Attributes_
Description
	Testing Anvil
	
Weight, lbs
	37.06

_Related Products_
Main: Concrete Test Hammer - English  (35-1475)
Main: Standard Concrete Test Hammer (35-1480)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Pulse Velocity Measurement
The basic principle of this method of testing is that the velocity of an ultrasonic pulse through concrete is related to its density and elastic properties. Some care is necessary when testing, but an experienced operator may obtain a considerable amount of information about a concrete member. The advantage of this method is that the pulse passes through the complete thickness of the concrete so that the significant defects can be detected. Pulse Velocity Measurement can be used for the following applications:  	* The measurement of concrete uniformity 	* Determination of the presence or absence of voids, cracks and other imperfections 	* Deterioration of the concrete which might haveoccurred due to age or through the action of fire,frost or chemical attack 	* Measurement of layer thickness and elastic modulus 	* Determination and monitoring of concrete strength

[PRODUCT GROUP] Pundit Lab

[PRODUCT] Ultrasound Couplant Supplied In 250ml bottle (35-2305)
Thick Grade

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Ultrasound Couplant

_Related Products_
Main: Pundit Lab Ultrasonic Concrete Tester  110-240V 50/60Hz 1Ph (35-2302/09)

[PRODUCT] Pundit Lab Ultrasonic Concrete Tester  110-240V 50/60Hz 1Ph (35-2302/09)
Pundit Lab is the most versatile Pundit to date. It has all the functions of the classic Pundit 7, but offers additional benefits.Designed with laboratory use in mind, its compact size, rugged construction and optimized power consumption make it equally suitable for on-site use.Along with the traditional transit time and pulse velocity measurement, Pundit Lab offers path length measurement, perpendicular crack depth measurement and surface velocity measurement.Optimized pulse shaping gives greater transmission range at lower voltage levels. This coupled with automated combination of the transmitter voltage and the receiver gain ensures an optimum received signal level, ensuring accurate and stable measurements.The waveform can be viewed either via an external oscilloscope connection or directly on a connected PC screen.Full remote control capability completes the package.Complete with two 54 kHz transducers each with 3.6 metres of cable, coupling agent, carrying case and instruction manual. 

_Further Information_
For 110 - 240 V AC, 50 - 60 Hz, 1 ph.

_Attributes_
Description
	Pundit Lab Ultrasonic Concrete Tester
	
Dimensions, l x w x h, ”
	12x18x6

_Related Products_
Spare/Consumable: Ultrasound Couplant Supplied In 250ml bottle (35-2305)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Compression Machines

[CATEGORY] Automatic Compression Machines
Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike. The machines to meet the requirements of EN 12390-3, -4, -5, 12504-1, 1354, 1521, 3161, 1338, 772-6, 13286-41 BS 3892-3, 187, 6717  

[PRODUCT GROUP] BS EN Compression Machines
* Machines to meet the requirements of EN 12390-3, -4, -5, 12504-1, 1354, 1521, 3161, 1338, 772-6, 13286-41 BS 3892-3, 187, 6717* Alpha-numeric keypad for data entry* Calibration accuracy to BS EN ISO 7500-1; ASTM E4* Automatic loading cycle* Wide range of accessories

[PRODUCT] ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
The ADR-Auto V2.0 2000 BS EN is supplied complete with self-centring lower platen and safety gates fitted with interlock switches ready for testing 300 x 150 mm diameter cylinders. When used for cube testing Distance pieces (EN) of the appropriate size must be ordered separately.

_Standards_
EN 12350-6, NF P18-411

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 50 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN 12390, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 50 Hz 1 Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	355 mm
	
Platen Sizes
	Lower 220mm sq,Upper 300mm dia
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Accessory: BS Block Platens & Platen Handling Assembly for 2000kN & 3000kN BS Frames. (37-4830)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[PRODUCT] ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
The ADR-Auto V2.0 2000 BS EN is supplied complete with self-centring lower platen and safety gates fitted with interlock switches ready for testing 300 x 150 mm diameter cylinders. When used for cube testing Distance pieces (EN) of the appropriate size must be ordered separately.

_Standards_
EN 12350-6

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 60 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN 12390, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 60 Hz 1 Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	355 mm
	
Platen Sizes
	Lower 220mm sq,Upper 300mm dia
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Accessory: BS Block Platens & Platen Handling Assembly for 2000kN & 3000kN BS Frames. (37-4830)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[PRODUCT] ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
The ADR-Auto V2.0 3000 BS EN is supplied complete with self-centring lower platen and safety gates fitted with interlock switches ready for testing 300 x 150 mm diameter cylinders. When used for cube testing Distance pieces (EN) of the appropriate size must be ordered separately.

_Standards_
EN 12350-6

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 60 Hz
	
Force Capacity, kN
	3000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN 12390, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Capacity
	3000 kN
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 60 Hz 1 Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	355 mm
	
Platen Sizes
	Lower 220mm sq,Upper 300mm dia
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 3000 kN Load Calibration Device Complete with Hand Held Readout Unit (37-8400)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Accessory: BS Block Platens & Platen Handling Assembly for 2000kN & 3000kN BS Frames. (37-4830)
Accessory: BS/EN Standard Rectangular Platen (37-4860)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[PRODUCT] ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
The ADR-Auto V2.0 3000 BS EN is supplied complete with self-centring lower platen and safety gates fitted with interlock switches ready for testing 300 x 150 mm diameter cylinders. When used for cube testing Distance pieces (EN) of the appropriate size must be ordered separately.

_Standards_
EN 12350-6, NF P18-411

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 50Hz
	
Force Capacity, kN
	3000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN 12390, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Capacity
	3000 kN
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 50 Hz 1 Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	355 mm
	
Platen Sizes
	Lower 220mm sq,Upper 300mm dia
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 3000 kN Load Calibration Device Complete with Hand Held Readout Unit (37-8400)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Accessory: BS Block Platens & Platen Handling Assembly for 2000kN & 3000kN BS Frames. (37-4830)
Accessory: BS/EN Standard Rectangular Platen (37-4860)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[GROUPED PRODUCT MATRIX]
Model No.
	EN 12390-6
	Voltage
	Capacity, kN
	Ram Travel
	N/A for this Product Group

[PRODUCT GROUP] General Purpose Compression Machines
* 2000 kN capacity * Tests 150 and 100 mm cubes and cylinders up to 320 x 160 mm diameter* Options to test and concrete beams to ASTM C78* Supplied with Windows download software as standard

[PRODUCT] ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
ADR-Auto V2.0 2000 Standard supplied complete with safety gates ready for testing 300 x 150 mm diameter cylinders. When used for cube testing distance pieces of the appropriate size must be ordered separately.

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V  50 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 150 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	n/a
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 50 Hz 1 Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	325 mm
	
Platen Sizes
	Lower , Upper 222 mm
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[PRODUCT] ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
ADR-Auto V2.0 2000 Standard supplied complete with safety gates ready for testing 300 x 150 mm diameter cylinders. When used for cube testing distance pieces of the appropriate size must be ordered separately.

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	100-120 V 60 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 150 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	n/a
	
TFV and ACV
	Yes
	
Voltage Supply
	110-120V 60Hz 1Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	341 mm
	
Max hor. Clearance
	326 mm
	
Platen Sizes
	Lower , Upper 222 mm
	
Max Ram Travel
	51 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 110 - 120 V AC, 60 Hz, 1 ph (37-6135/02)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[PRODUCT] ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
ADR-Auto V2.0 2000 Standard supplied complete with safety gates ready for testing 300 x 150 mm diameter cylinders. When used for cube testing distance pieces of the appropriate size must be ordered separately.

_Further Information_
**Not available for sale in the USA** Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.ACCURACY & SAVINGSThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.TRACEABILITY & DATA QUALITYThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.USER SAFETYFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 60 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50

_Specification_
Testing Standards
	BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 150 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	n/a
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 60 Hz 1 Ph
	
Frame Type
	Welded
	
Max vert. Clearance
	342 mm
	
Max hor. Clearance
	327 mm
	
Platen Sizes
	Lower , Upper 222 mm
	
Max Ram Travel
	52 mm

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	Capacity, kN
	Ram Travel
	N/A for this Product Group

[PRODUCT GROUP] Dual Frame Compression Machines
Designed to provide comprehensive test facilities, dual-frame compressions enable a versatile testing programme. Controlled by a single console, dual-frame compression machines provide an economic means of testing the full range of concrete, mortar and cement samples

[PRODUCT] ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
* 2000/250 kN capacity* Meets requirements of EN 12390-3, -4, -12504-1, 1354, 1521, 13161, 1338 772- 1, -6, 13286-41 196- 1 459-2. BS 3892-3, 187* Concrete and cement specimens* Tests 200, 150, 100, 70.7, 50 and 40 mm cubes and cylinders up to 320 x 160 mm diameter* Calibration accuracy and repeatability conforms to BS EN ISO 7500-1; ASTM E4* Supplied with Windows(R) download software as standardDesigned to provide comprehensive test facilities, this twin-frame compression machine is controlled by the automatic console. The 2000 kN capacity frame meets the requirements of EN Standards and accepts the range of on-board accessories.As the second outlet control port is connected to the 250 kN load frame, attachment of a flexural frame is not possible. The 250 kN frame is supplied complete with compression jig, 40 mm, 50 mm/2.0 inch square platens and meets the requirements of EN 196-1. When selecting the frame to be used for testing the automatic changeover valve incorporated in the system delivers the hydraulic fluid to that frame.

_Standards_
EN 12350-6, EN 196-1

_Further Information_
**Not available for sale in the USA** 220-240V 50Hz 1Ph.

_Attributes_
Frame 1
	2000 kN
	
Frame 2
	250 kN
	
Voltage Supply
	220-240 V 50 Hz

_Specification_
Testing Standards
	BS EN 12390-3, BS EN 12390-4, EN 12504-1, EN 1354, EN 1521, EN 13161, EN1338, EN 772-1, EN 772-6, EN 13286-41, EN 196- 1, EN 459-2, BS 3892-3, BS 187
	
Voltage Supply
	220-240 V 50 Hz 1 Ph

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)
Accessory: BS/EN Standard Rectangular Platen (37-4860)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Extended Front Safety Gate for Use with 2000kN BS/EN Load Frames Fitted with Rectangular Platens. (37-4835)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[PRODUCT] ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
* 2000/250 kN capacity* Meets requirements of EN 12390-3, -4, -12504-1, 1354, 1521, 13161, 1338 772- 1, -6, 13286-41 196- 1 459-2. BS 3892-3, 187* Concrete and cement specimens* Tests 200, 150, 100, 70.7, 50 and 40 mm cubes and cylinders up to 320 x 160 mm diameter* Calibration accuracy and repeatability conforms to BS EN ISO 7500-1; ASTM E4* Supplied with Windows(R) download software as standardDesigned to provide comprehensive test facilities, this twin-frame compression machine is controlled by the automatic console. The 2000 kN capacity frame meets the requirements of EN Standards and accepts the range of on-board accessories.As the second outlet control port is connected to the 250 kN load frame, attachment of a flexural frame is not possible. The 250 kN frame is supplied complete with compression jig, 40 mm, 50 mm/2.0 inch square platens and meets the requirements of EN 196-1. When selecting the frame to be used for testing the automatic changeover valve incorporated in the system delivers the hydraulic fluid to that frame.

_Standards_
EN 12350-6, EN 196-1

_Further Information_
**Not available for sale in the USA** 220-240V 60Hz 1Ph.

_Attributes_
Frame 1
	2000 kN
	
Frame 2
	250 kN
	
Voltage Supply
	220-240 V 60 Hz

_Specification_
Testing Standards
	BS EN 12390-3, BS EN 12390-4, EN 12504-1, EN 1354, EN 1521, EN 13161, EN1338, EN 772-1, EN 772-6, EN 13286-41, EN 196- 1, EN 459-2, BS 3892-3, BS 187
	
Voltage Supply
	220-240 V 60 Hz 1 Ph

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Accessory: BS/EN Standard Rectangular Platen (37-4860)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Extended Front Safety Gate for Use with 2000kN BS/EN Load Frames Fitted with Rectangular Platens. (37-4835)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[PRODUCT] ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)
* 3000/250 kN capacity* Meets requirements of EN 12390-3, -4, -12504-1, 1354, 1521, 13161, 1338 772- 1, -6, 13286-41 196- 1 459-2. BS 3892-3, 187* Concrete and cement specimens* Tests 200, 150, 100, 70.7, 50 and 40 mm cubes and cylinders up to 320 x 160 mm diameter* Calibration accuracy and repeatability conforms to BS EN ISO 7500-1; ASTM E4* Supplied with Windows(R) download software as standardDesigned to provide comprehensive test facilities, this twin-frame compression machine is controlled by the automatic console. The 3000 kN capacity frame meets the requirements of EN Standards and accepts the range of on-board accessories.As the second outlet control port is connected to the 250 kN load frame, attachment of a flexural frame is not possible. The 250 kN frame is supplied complete with compression jig, 40 mm, 50 mm/2.0 inch square platens and meets the requirements of EN 196-1. When selecting the frame to be used for testing the automatic changeover valve incorporated in the system delivers the hydraulic fluid to that frame.

_Standards_
EN 12350-6, EN 196-1

_Further Information_
**Not available for sale in the USA** 220-240V 50Hz 1Ph.

_Attributes_
Frame 1
	3000 kN
	
Frame 2
	250 kN
	
Voltage Supply
	220-240 V 50 Hz

_Specification_
Frame
	Frame 1, Frame 2
	
Standards
	EN 12390, EN 196
	
Frame Type
	Welded, Welded
	
Capacity
	3000 kN, 250 kN
	
Max Vert. Clearance
	340 mm, 230 mm
	
Max Hor. Clearance
	310 mm, 160 mm
	
Platen Size
	Lower 220 mm sq.Upper 300 mm dia., 150 mm dia.
	
Max Ram Travel
	50 mm, 15 mm
	
Samples
	 ,  
	
Cube Sample Size
	Up to 200 mm, -
	
Cylinder Sample Size
	Up to 160 x 320 mm, Up to 100 mm
	
Blocks
	Via optional Platen Handling System, n/a
	
40 mm, 50 mm (2") Cubes
	n/a, Yes
	
40.1 x 40 x 160 mm (Compression)
	n/a, Yes
	
TFV & ACV
	Yes, n/a
	
Hydraulics
	 ,  
	
Rapid Approach
	Yes, Not Required
	
Hydraulic Pump
	Variable Output, Variable Output
	
Data Comms
	 ,  
	
Printer, PC Download, USB, RS232
	Yes, Yes
	
Screen
	 ,  
	
145 mm (5.7") Touch Screen w/ Graphical Display
	Yes, Yes
	
Platens
	 ,  
	
3rd Party Certified
	Yes, Yes
	
Misc
	 ,  
	
Sample Alignment
	Location Fixtures, Location Fixtures
	
Pace Rate Indicator
	Yes, Yes
	
Load Time v Goodness of Test
	Yes, Yes
	
Analysis of Trend Data
	Yes, Yes
	
Memory of Test Results
	Yes, Yes

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[GROUPED PRODUCT MATRIX]
Model No.
	EN 12390-6
	EN 196-1
	Frame 1
	Frame 2
	Voltage
	N/A for this Product Group

[CATEGORY] Manually-Operated Compression Machines
The new ADR Touch Series, with 145mm (5.7") high resolution QVGA touch screen interface and intuitive menu-driven operation, reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%.  	* Up to 6 sample types can be set as favorites, enabling one-touch set up for repeat testing.	* Full, QWERTY touch pad for input of test data.Most testing errors produce lower strength results. Non-compliant loading rates can generate errors in measured strength. The user interface includes real-time display of load vs. time, further ensuring accurate and consistent test results and providing "goodness of test" data to improve traceability in your QC operations.TRACEABILITY & DATA QUALITYThe ADR range now provides improved data quality and traceability in due diligence cases - it is now possible to demonstrate traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. 	* Enhanced USB data communications between PC and machine - eliminating the need for download software. 	* Two gigabytes of storage memory. 	* Full customization of sample sizes - stress calculations are automatically recalculated.

[PRODUCT GROUP] BS EN Compression Machines
* 2000 and 3000 kN capacity* Optional platen handling systems which include BS 6073-1, EN 772-1 specification rectangular platens* Machines to meet the requirements of EN 12390-3, -4, -5, 12504-1, 1354, 1521, 3161, 1338, 772-6, 13286-41 BS 3892-3, 187, 6717* Tests 200, 150 and 100 mm cubes and cylinders up to 320 x 160 mm diameter* Supplied with Windows(R) download software as standard

[PRODUCT] ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
The ADR Touch range of 2000 kN and 3000 kN capacity compression machines has been designed to meet the need for reliable and consistent testing. The load frame is a welded steel fabrication carrying the ball-seated upper platen. Positively located on the loading ram, which is protected from debris by a flexible cover, the lower platen is marked for the centring of cube and cylinder specimens. Self-centring lower platens for cube location are supplied as standard on EN machines and are available as an optional extra on the standard machine. The two machines for cube testing to EN standards are assembled and aligned using a special compression frame stability tester.The dimensions of the frame allow the testing of concrete cylinders up to 320 mm long x 160 mm diameter, 150 and 100 mm square cubes, and on EN/BS machines, 200 mm square cubes. Kerbs and flagstones may also be tested on ADR machines as well as 150 mm and 100 mm square section beams to ASTM C78 using the optional 100 kN flexural frames which are connected to the power pack.

_Standards_
EN 12350-6, NF P18-411

_Further Information_
**Not available for sale in the USA** ADR Touch BS EN 2000 and 3000 kN compression machines are supplied complete with self-centring lower platen and safety gates fitted with interlock switches ready for testing 300 x 150 mm diameter cylinders.Whilst delivering all the features and reputation of the established ADR Series with its extensive design history, the new and improved user interface provides a high quality platform for testing that enhances the performance of ELE's compression machines.New, sophisticated electronics further the benefits of simplified operation, whilst delivering the highest levels of accuracy in testing concrete and cement/mortar samples, satisfying the needs of Quality Control Managers, Lab Managers and Technicians.ACCURACY & SAVINGSThe new ADR Touch Series, with 145mm (5.7") high resolution QVGA touch screen interface and intuitive menu-driven operation, reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%.* Up to 6 sample types can be set as favorites, enabling one-touch set up for repeat testing.* Full, QWERTY touch pad for input of test data.Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. The user interface includes real-time display of load vs. time, further ensuring accurate and consistent test results and providing "goodness of test" data to improve traceability in your QC operations.TRACEABILITY & DATA QUALITYThe ADR range now provides improved data quality and traceability in due diligence cases - it is now possible to demonstrate traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached.* Enhanced USB data communications between PC and machine - eliminating the need for download software.* Two gigabytes of storage memory.* Full customization of sample sizes - stress calculations are automatically recalculated.USER SAFETYWith full safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure thesafety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 50/60 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50 mm

_Specification_
Testing Standards
	BS EN 12390-4, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
Flexural Testing
	Via Flexural Frame
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240V 50/60 Hz 1Ph.
	
Frame Class (Stability)
	Tested
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	355 mm
	
Platen Sizes
	Lower 220mm sq,Upper 300mm dia
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Accessory: ADR Touch Head for Compression machines (37-4950/09)
Accessory: BS/EN Standard Rectangular Platen (37-4860)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Extended Front Safety Gate for Use with 2000kN BS/EN Load Frames Fitted with Rectangular Platens. (37-4835)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[PRODUCT] ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
The ADR Touch range of 2000 kN and 3000 kN capacity compression machines has been designed to meet the need for reliable and consistent testing. The load frame is a welded steel fabrication carrying the ball-seated upper platen. Positively located on the loading ram, which is protected from debris by a flexible cover, the lower platen is marked for the centring of cube and cylinder specimens. Self-centring lower platens for cube location are supplied as standard on EN machines and are available as an optional extra on the standard machine. The two machines for cube testing to EN standards areassembled and aligned using a special compression frame stability tester.The dimensions of the frame allow the testing of concrete cylinders up to 320 mm long x 160 mm diameter, 150 and 100 mm square cubes, and on EN/BS machines, 200 mm square cubes. Kerbs and flagstones may also be tested on ADR machines as well as 150 mm and 100 mm square section beams to ASTM C78 using the optional 100 kN flexural frames which are connected to the power pack.

_Standards_
EN 12350-6, NF P18-411

_Further Information_
**Not available for sale in the USA** ADR Touch BS EN 2000 and 3000 kN compression machines are supplied complete with self-centring lower platen and safety gates fitted with interlock switches ready for testing 300 x 150 mm diameter cylinders.Whilst delivering all the features and reputation of the established ADR Series with its extensive design history, the new and improved user interface provides a high quality platform for testing that enhances the performance of ELE's compression machines.New, sophisticated electronics further the benefits of simplified operation, whilst delivering the highest levels of accuracy in testing concrete and cement/mortar samples, satisfying the needs of Quality Control Managers, Lab Managers and Technicians.ACCURACY & SAVINGSThe new ADR Touch Series, with 145mm (5.7") high resolution QVGA touch screen interface and intuitive menu-driven operation, reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%.* Up to 6 sample types can be set as favorites, enabling one-touch set up for repeat testing.* Full, QWERTY touch pad for input of test data.Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. The user interface includes real-time display of load vs. time, further ensuring accurate and consistent test results and providing "goodness of test" data to improve traceability in your QC operations.TRACEABILITY & DATA QUALITYThe ADR range now provides improved data quality and traceability in due diligence cases - it is now possible to demonstrate traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached.* Enhanced USB data communications between PC and machine - eliminating the need for download software.* Two gigabytes of storage memory.* Full customization of sample sizes - stress calculations are automatically recalculated.USER SAFETYWith full safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure thesafety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 50/60 Hz
	
Force Capacity, kN
	3000
	
Maximum Ram Travel mm
	50 mm

_Specification_
Testing Standards
	BS EN 12390-4, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Capacity
	3000 kN
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
Flexural Testing
	Via Flexural Frame
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240V 50/60 Hz 1Ph.
	
Frame Class (Stability)
	Tested
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	310 mm
	
Platen Sizes
	Lower 220mm sq,Upper 300mm dia
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
Accessory: 3000 kN Load Calibration Device Complete with Hand Held Readout Unit (37-8400)
Accessory: ADR Touch Head for Compression machines (37-4950/09)
Accessory: BS/EN Standard Rectangular Platen (37-4860)
Accessory: EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)
Accessory: EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)
Accessory: EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)
Accessory: EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

[GROUPED PRODUCT MATRIX]
Model No.
	EN 12390-6
	Voltage
	Capacity, kN
	Ram Travel
	N/A for this Product Group

[PRODUCT GROUP] General Purpose Compression Machines
* 1560 kN/350 000 lbf and 2000 kN/450 000 lbf capacity* Tests 150 and 100 mm cubes, or cylinders up to 320 x 160 mm diameter* ADR Touch Digital readout in kN/lbf/kgf* Supplied with Windows(R) download software as standard* Calibration accuracy to BS EN ISO 7500-1; ASTM E4;* Efficient hydraulic power packs* Economic machines ideal for site use

[PRODUCT] ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
* 1560 kN/350 000 lbf capacity* Calibration accuracy to BS EN ISO 7500-1; ASTM E4;* Efficient hydraulic power packs* Economic machines ideal for site useThe Compact 1500 range of compression machines has been designed to meet the need for a simple, economic and reliable means of testing concrete.SPECIMEN CAPACITYThe dimensions of the frame allow the testing of cylinders up to 320 mm long x 160 mm diameter, and cubes 150 or 100 mm square. Kerbs and flagstones may also be tested on the ADR machine as well as 150 mm and 100 mm square section beams to ASTM C78, using the optional 100 kN flexural frames which are connected to the power pack.LOAD INDICATIONThe ADR digital readout is a microprocessor controlled instrument, which is fitted as standard to all digital machines in the range. Load can be displayed in kN, lbf or kgf as selected by the operator.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** The Standard range of compression machines has been designed to meet the need for a simple, economic and reliable means of testing concrete.Whilst delivering all the features and reputation of the established ADR Series with its extensive design history, the new and improved user interface provides a high quality platform for testing that enhances the performance of ELE's compression machines.New, sophisticated electronics further the benefits of simplified operation, whilst delivering the highest levels of accuracy in testing concrete and cement/mortar samples, satisfying the needs of Quality Control Managers, Lab Managers and Technicians.ACCURACY & SAVINGSThe new ADR Touch Series, with 145mm (5.7") high resolution QVGA touch screen interface and intuitive menu-driven operation, reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%.* Up to 6 sample types can be set as favorites, enabling one-touch set up for repeat testing.* Full, QWERTY touch pad for input of test data.Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. The user interface includes real-time display of load vs. time, further ensuring accurate and consistent test results and providing "goodness of test" data to improve traceability in your QC operations.TRACEABILITY & DATA QUALITYThe ADR range now provides improved data quality and traceability in due diligence cases - it is now possible to demonstrate traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached.* Enhanced USB data communications between PC and machine - eliminating the need for download software.* Two gigabytes of storage memory.* Full customization of sample sizes - stress calculations are automatically recalculated.USER SAFETYWith full safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 50/60 Hz
	
Force Capacity, kN
	1500
	
Maximum Ram Travel mm
	50 mm

_Specification_
Testing Standards
	BS EN ISO 7500-1, ASTM E4
	
Capacity
	1500 kN
	
Cubes (Concrete)
	Up to 150 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	n/a
	
Flexural Testing
	Via Flexural Frame
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240V 50/60 Hz 1Ph.
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	325 mm
	
Platen Sizes
	Lower, Upper 222 mm
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Accessory: ADR Touch Head for Compression machines (37-4950/09)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[PRODUCT] ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
* 2000 kN/450 000 lbf capacity* Tests 150 and 100 mm concrete cubes or cylinders up to 320 x 160 mm diameter* Supplied with Windows(R) download software as standard.Incorporating the ADR Touch digital readout, the machines are designed to test cubes and cylinders in accordance with most International Standards. Supplied fitted for cylinder testing with safety gates. When used for cube testing appropriate distance pieces according to the size of specimen to be tested are required and must be ordered separately.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** The Standard range of compression machines has been designed to meet the need for a simple, economic and reliable means of testing concrete.Whilst delivering all the features and reputation of the established ADR Series with its extensive design history, the new and improved user interface provides a high quality platform for testing that enhances the performance of ELE's compression machines.New, sophisticated electronics further the benefits of simplified operation, whilst delivering the highest levels of accuracy in testing concrete and cement/mortar samples, satisfying the needs of Quality Control Managers, Lab Managers and Technicians.ACCURACY & SAVINGSThe new ADR Touch Series, with 145mm (5.7") high resolution QVGA touch screen interface and intuitive menu-driven operation, reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%.* Up to 6 sample types can be set as favorites, enabling one-touch set up for repeat testing.* Full, QWERTY touch pad for input of test data.Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. The user interface includes real-time display of load vs. time, further ensuring accurate and consistent test results and providing "goodness of test" data to improve traceability in your QC operations.TRACEABILITY & DATA QUALITYThe ADR range now provides improved data quality and traceability in due diligence cases - it is now possible to demonstrate traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached.* Enhanced USB data communications between PC and machine - eliminating the need for download software.* Two gigabytes of storage memory.* Full customization of sample sizes - stress calculations are automatically recalculated.USER SAFETYWith full safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Voltage Supply
	220-240 V 50/60 Hz
	
Force Capacity, kN
	2000
	
Maximum Ram Travel mm
	50 mm

_Specification_
Testing Standards
	BS EN ISO 7500-1, ASTM E4
	
Capacity
	2000 kN
	
Cubes (Concrete)
	Up to 150 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	n/a
	
Flexural Testing
	Via Flexural Frame
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240V 50/60 Hz 1Ph.
	
Frame Type
	Welded
	
Max vert. Clearance
	340 mm
	
Max hor. Clearance
	325 mm
	
Platen Sizes
	Lower, Upper 222 mm
	
Max Ram Travel
	50 mm

_Related Products_
Accessory: 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
Accessory: 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Accessory: ADR Touch Head for Compression machines (37-4950/09)
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Spare/Consumable: Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[GROUPED PRODUCT MATRIX]
Model No.
	Voltage
	Capacity, kN
	Ram Travel
	N/A for this Product Group

[CATEGORY] Compression/Tension Testing

[PRODUCT GROUP] Compression Tension Machine

[PRODUCT] 1000/500kN Motorised Compression/Tension Machine  (complete with grips) 220-240V 50/60Hz 1Ph. (36-1410/01)
* Compression testing of concrete cubes and cylinders* Calibration in compression is accurate to 1% of indicated load, satisfying BS EN ISO 7500-1; ASTM E4 * Self-aligning upper platen for compression tests* Easily fitted grips for tension testingThe load frame is of high quality steel construction with a fixed upper head carrying a ball-seated platen. The ram carrying the lower platen is contained in the base of the frame and is protected by a shroud. Sufficient clearance between the platens allows the compression testing of concrete cylinders up to 160 mm diameter by 320 mm long. To allow for the compression testing of concrete cubes, a range of distance pieces is available.Tension tests on steel reinforcing bars are conducted by replacing the platens with special grips. As standard the machine is supplied with the following size grips for testing bars, 10 mm, 12 mm, 20 mm, and 25 mm diameter. The machine is motorised, incorporating a change-over lever to select either compression or tension output from the pump.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** 220-240V 50/60 Hz 1Ph.

_Attributes_
Description
	Motorised Compression/Tension Machine
	
Voltage Supply
	220-240 V 50/60 Hz

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Voltage
	N/A for this Product Group

[CATEGORY] Compression Machines Accessories
The selection and use of the correct accessories is essential if the range of machines described in the Compression Machines section is to be utilised to its full advantage.This section details a wide range of accessory items including distance pieces, specialist platens, flexural testing frames and other devices.

[PRODUCT GROUP] Strain Gauge

[PRODUCT] 200mm "Demec" Mechanical Strain Gauge (35-2846)
This gauge is ideal for monitoring cracks and strains in a number of structure types.

_Standards_
BS 1881-206

_Attributes_
Description
	Demec Mechanical Strain Gauge - 200 mm

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Distance Pieces
Distance pieces are used to reduce the amount of vertical space between the upper platen and the top surface of the specimen.Two versions are offered, both of which have a maximum load capacity of 3000 kN and are for use with fixed head load frames.

[PRODUCT] Standard Distance Piece -  20 mm Depth (37-4980)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	Standard
	
Distance piece depth, mm
	20

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ELE-Hoek Cell ADR Touch 2000 Compression Machine. 220 - 240 V 50/60H z (70-2630/01)
Main: Ele-Hoek Cell Nx 54.74mm Diameter. (70-1710)
Main: Hand Operated Pressure System. Complete with Pressure Gauge and Flexible Hose. (70-5000)
Main: Pressure Test 3500 Oil/Water Constant Pressure System with Digital Pressure Gauge. (70-5130/01)

[PRODUCT] Standard Distance Piece -  50 mm Depth (37-5000)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	Standard
	
Distance piece depth, mm
	50

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)

[PRODUCT] Standard Distance Piece -  60 mm Depth (37-5020)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	Standard
	
Distance piece depth, mm
	60

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)

[PRODUCT] Standard Distance Piece -  80 mm Depth (37-5050)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	Standard
	
Distance piece depth, mm
	80

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)

[PRODUCT] Standard Distance Piece -  100 mm Depth (37-5100)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	Standard
	
Distance piece depth, mm
	100

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)

[PRODUCT] EN 12390-3/4 Distance Piece -  20 mm Depth (37-5110)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	BS EN
	
Distance piece depth, mm
	20

_Related Products_
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)

[PRODUCT] EN 12390-3/4 Distance Piece -  50 mm Depth (37-5120)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	BS EN
	
Distance piece depth, mm
	50

_Related Products_
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)

[PRODUCT] EN 12390-3/4 Distance Piece -  60 mm Depth (37-5140)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	BS EN
	
Distance piece depth, mm
	60

_Related Products_
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)

[PRODUCT] EN 12390-3/4 Distance Piece -  80 mm Depth (37-5170)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	BS EN
	
Distance piece depth, mm
	80

[PRODUCT] EN 12390-3/4 Distance Piece -  100 mm Depth (37-5180)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Compression machine type
	BS EN
	
Distance piece depth, mm
	100

_Related Products_
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Machine type
	Depth, mm
	N/A for this Product Group

[PRODUCT GROUP] Platen Assemblies
All ELE compression machines are supplied as standard with relevant platen assemblies. The versatility of the machines is such that other tests may be performed in addition to the main application. Often these tests will require different platens, e.g. for block testing. ELE offers a range of optional platen assemblies which are quickly fitted for use.

[PRODUCT] BS Block Platens & Platen Handling Assembly for 2000kN & 3000kN BS Frames. (37-4830)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	BS Block Platens & Platen Handling Assembly

_Related Products_
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)

[PRODUCT] Extended Front Safety Gate for Use with 2000kN BS/EN Load Frames Fitted with Rectangular Platens. (37-4835)
For use with 2000 kN capacity machines fitted with rectangular platens.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Extended front safety gate for use with rectangular platens

_Related Products_
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)

[PRODUCT] BS/EN Standard Rectangular Platen (37-4860)
Manufactured to the requirements of BS 6073-1 and EN 772-1 these platens, measuring 445 x 250 x 75 mm thick, are suitable for testing a wide range of samples. The upper platen is clipped to the machine's standard ball seating assembly. The platens are supplied complete with 2 bolt-on spacers for use when testing blocks of 140 mm or 190 mm height. Maximum vertical clearance is 245 mm.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	BS EN Rectangular platens for block testing

_Related Products_
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)

[PRODUCT] Test Pieces EN 12390-6 Pack of 100 Hardboard. (37-5450)
Hardboard strips for use with Split Cylinder Platen Assemblies. Pack of 100.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Test pieces for splitting tensile test

[PRODUCT] Sub-Platen Assembly for 150mm Dia Specimens for Split Cylinder Testing to BS1881 / EN12390-6 (37-5420)
For testing cylinders of 150 x 150 mm and 150 x 300 mm (diameter x length).

_Standards_
EN 12350-6

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Platens for tensile splitting of cylinders

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Printing of results

[PRODUCT] Paper Roll 76mm Wide (Box of 20) (37-4859/12)
Pack of 10 rolls.

_Attributes_
Description
	Paper Roll

_Related Products_
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)

[PRODUCT] Printer Ribbon(Black/Red) for Use with Impact Printer. (37-4859/10)

_Attributes_
Description
	Printer Ribbon

_Related Products_
Accessory: Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)

[PRODUCT] Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/02)
Supplied complete with serial RS232 communications cable and one paper roll.

_Further Information_
100 - 120 V AC, 60 Hz, 1 ph.

_Attributes_
Description
	Impact Printer RS232 Serial Connection

[PRODUCT] Impact Printer Rs232 Serial Connection. Supplied Complete with 1 Paper Roll. (37-4859/01)
Supplied complete with serial RS232 communications cable and one paper roll.

_Further Information_
**Not available for sale in the USA** 220 - 240 V AC, 50 - 60 Hz, 1 ph.

_Attributes_
Description
	Impact Printer

_Related Products_
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)
Spare/Consumable: Paper Roll 76mm Wide (Box of 20) (37-4859/12)
Spare/Consumable: Printer Ribbon(Black/Red) for Use with Impact Printer. (37-4859/10)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Compression Machine Upgrades
Upgrade your ELE compression machines to enjoy the features of the ADR Touch and ADR Auto V2.0 range.

[PRODUCT] Console Assy ADR-Auto V2.0 (37-4880/01)
For upgrading ELE concrete compression machines manufactured after 1983. For 220 - 240 V, 50 Hz, 1 ph.

_Further Information_
**Not available for sale in the USA** 220-240V 50Hz

_Attributes_
Description
	To upgrade an existing "AutoTest" to ADR Auto V2.0

[PRODUCT] ADR Touch Head Kit to upgrade manual compression machines (37-4990/09)
Following the introduction of the new range of ADR Touch compression machines, ELE are pleased to announce the release of an upgrade package for existing machines.This package is suitable for a wide range of ELE manually-controlled machines in service (contact our service department for details) and in most cases can fit directly to the existing machine.Supplied complete in colour matched housing with all fittings and new replacement high quality pressure transducer this system enables users to take advantage of the latest touch screen technology plus enhanced data facilities.

_Further Information_
**Not available for sale in the USA** 110 - 240 V, AC 50 - 60 Hz, 1 ph.

_Attributes_
Description
	To upgrade existing ADR machines to ADR Touch

[PRODUCT] Kit to Upgrade ADR-Auto Compression m/c to V2.0 (37-4900/01)
The ADR-Auto with console no. 1903B0001 can be upgraded by purchasing kit no. 37-4900/01 that contains the new ADR Auto V2.0 digital controller and a new transducer. Please be aware that the machine will need to be recalibrated. Whilst delivering all of the features and reputation of the established ADR-Auto V2.0 range with its 20 year design history, the new and improved user interface provides a high quality platform for testing that will enhance the performance of our compression machines. New, sophisticated electronics further the benefits of a closed-loop operation in testing concrete and cement/ mortar samples, satisfying the requirements of Quality Control Managers, Lab Managers and Technicians alike.  

_Further Information_
**Not available for sale in the USA** 220-240V 50/60Hz Accuracy & SavingsThe NEW ADR-Auto V2.0 range, with 145mm (5.7") touch screen interface and intuitive menu driven operation reduces the time taken to set up the machine and perform tests, reducing the time to train staff by up to 25%. Most testing errors produce lower strength results. Noncompliant loading rates can generate errors in measured strength. With the latest closed-loop technology used in the ADR-Auto V2.0, the most effective cement ratios can be used with confidence.Traceability & Data QualityThe ADR-Auto V2.0 now provides improved data quality and traceability in due diligence cases - it is now possible to display traceability all the way from the machine/user to the accreditation body, increasing your reputation and peace of mind - all test results now come complete with the machine serial number attached. Prove your service quality - the ADR-Auto V2.0 now plots load vs time in real-time, proving full compliance to the testing standard. This data can be stored for later use or for detailed analysis of the concrete production.User SafetyFull safety gates as standard, total systems diagnostics, ram run-out switches and overload warnings ensure the safety of your employees and the reliability of your machine.

_Attributes_
Description
	To upgrade ADR-Auto machines to ADR Auto V2.0

_Specification_
Testing Standards
	BS EN 12390, BS EN 12390-3, BS EN 12390-4, BS EN 12390-5, EN 12504-1, EN 1354, EN 1521, EN 3161, EN 1338, EN 772-6, EN 13286-41, BS 3892-3, BS 187, BS 6717, BS EN ISO 7500-1, ASTM E4
	
Cubes (Concrete)
	Up to 200 mm
	
Cylinders (Concrete)
	Up to 160 x 320 mm
	
Blocks
	Via optional Platen Handling System
	
TFV and ACV
	Yes
	
Voltage Supply
	220-240 V 50 Hz 1 Ph

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Calibration Devices
* Calibrated to BS EN ISO376 Grade 1* 2000 & 3000 kN capacity* 7½ digit high-resolution hand-held readout* Designed for the calibration and verification of concrete compression machinesThe ELE electronic 2000 kN load cell and readout unit is an accurate and sensitive system for the calibration and verification of the load measuring systems of concrete compression machines. Each system is supplied complete with NPL (National Physical Laboratory UK) calibration certificate in compliance with BS EN ISO376 Grade 1.

[PRODUCT] 2000 kN Capacity Calibration Load Cell with Hand-Held Readout (37-8315)
Supplied with rechargeable batteries and universal charger.

_Further Information_
**Not available for sale in the USA** 110 - 240 V, AC 50 - 60 Hz, 1 ph.

_Attributes_
Description
	2000 kN capacity calibration device

_Related Products_
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)

[PRODUCT] 3000 kN Load Calibration Device Complete with Hand Held Readout Unit (37-8400)
Supplied with rechargeable batteries and universal charger.

_Further Information_
**Not available for sale in the USA** 110 - 240 V, AC 50 - 60 Hz, 1 ph.

_Attributes_
Description
	3000 kN capacity calibration device

_Related Products_
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Spares

[PRODUCT] Pressure transducer, 0-700bar, 0.05 to 10v DC Output (6014A0062)

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Pressure transducer

_Related Products_
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Flexural and Transverse Machines and Accessories
The flexural and transverse strength of concrete is of interest to engineers for many reasons. Movement of strucutres which may be induced by e.g. Temperature changes, ground vibrations, cyclic loading of road pavements and many other external influences, will set up internal stresses within a concrete member. Modern concrete technology utilises a wide range of materials such as glass or steel fibres to improve the flexural strength of the concrete. These modified concretes often require the use of special tests and equipment. Lower loads are used to test concrete in flexure; however, the shape and size of test specimens is such that larger and often heavy specimens can be difficult to handle. ELE has designed the range of machines offered to provide for ease of specimen positioning and subsequent testing. The range of flexural test equipment offered provides a wide variety of choice and test methods including low strength compression tests using optional ball seating assemblies.

[PRODUCT GROUP] Flexural and Transverse Testing

[PRODUCT] 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
* Open sided for ease of specimen loading* Meets EN 1339, 1340 for kerbs and flagstones* Optional ball seating assemblyThis rigidly constructed, open sided frame is suitable for testing kerbs and flagstones to EN 1339,1340. With optional accessories it can also be used to test 100 mm and 150 mm section beams for flexural strength to EN 12390-5.The frame supports a hydraulic ram and upper subplaten assembly incorporating spherical seating. The upper and lower sub-platens will accept specimen loading bearers, which are supplied separately.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	100kN Flexural and Transverse (Flags) Frame

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 110 - 120 V AC, 60 Hz, 1 ph (37-6135/02)
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
Accessory: Ball Seating Assembly 150mm Dia Platens. (37-6133)
Accessory: Specimen Bearer Assembly (37-6330)
Accessory: Specimen Bearers for Testing Flags. Used on 37-6140 Flags Frame. (37-6364)
Accessory: Specimen Bearers for Testing KerBS. Used on 37-6140 Flags Frame. (37-6362)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[PRODUCT] Specimen Bearer Assembly (37-6330)
EN 12390-5, 1521, 13161, 772-6. Comprising 2 self-aligning upper roller bearers, 1 self-aligning and 1 fixed lower roller bearer. Roller bearers are 38 mm dia x 320 mm long and suitable for 3- or 4-point flexural testing of beams.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Specimen Bearer Assembly for flexural testing of beams

_Related Products_
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)

[PRODUCT] Specimen Bearers for Testing KerBS. Used on 37-6140 Flags Frame. (37-6362)
For transverse testing of kerbs to EN 1340.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Specimen Bearers for transverse testing of kerbs

_Related Products_
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)

[PRODUCT] Specimen Bearers for Testing Flags. Used on 37-6140 Flags Frame. (37-6364)
For transverse testing of flags to EN 1339.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Specimen Bearers for transverse testing of flags

_Related Products_
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Flexural Testing for Beams

[PRODUCT] 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
* Open sided for ease of specimen loading* Meets EN 12390-5, 1521, 13161, 772-6 and ASTM C78 for standard section beams* Optional ball seating assemblyThis rigidly constructed, open sided frame is suitable for testing 100 mm and 150 mm square-section beams. The frame supports a hydraulic ram and upper sub-platen assembly incorporating a spherical seating. The upper and lower sub-platens will accept various specimen loading bearers, which are supplied separately.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	100kN Flexural (Beams) Frame

_Related Products_
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 110 - 120 V AC, 60 Hz, 1 ph (37-6135/02)
Accessory: 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
Accessory: 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
Accessory: ASTM C78 Specimen Bearer Assembly Case-Hardened 38mm Dia X 160mm Length. (37-6132)
Accessory: Ball Seating Assembly 150mm Dia Platens. (37-6133)
Accessory: BS 1881 Specimen Bearer Assembly 38mm Dia X 160mm Length. (37-6131)
Accessory: Standard Distance Piece -  100 mm Depth (37-5100)
Accessory: Standard Distance Piece -  20 mm Depth (37-4980)
Accessory: Standard Distance Piece -  50 mm Depth (37-5000)
Accessory: Standard Distance Piece -  60 mm Depth (37-5020)
Accessory: Standard Distance Piece -  80 mm Depth (37-5050)

[PRODUCT] BS 1881 Specimen Bearer Assembly 38mm Dia X 160mm Length. (37-6131)
Comprising 2 self-aligning upper bearers, 1 self-aligning and 1 fixed lower bearer. Roller bearers are 38 mm diameter x 160 mm long. Suitable for 3- or 4-point flexural testing of beams.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Specimen Bearers for flexural testing of beams EN

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)

[PRODUCT] ASTM C78 Specimen Bearer Assembly Case-Hardened 38mm Dia X 160mm Length. (37-6132)
Comprising 2 self-aligning upper bearers, 1 self-aligning and 1 fixed lower bearer; case-hardened, 38 mm diameter x 160 mm long and suitable for 3- or 4-point flexural testing of beams.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Specimen Bearers for flexural testing of beams ASTM

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)

[PRODUCT] Ball Seating Assembly 150mm Dia Platens. (37-6133)
Comprising a ball seating assembly with 150 mm diameter platen and a lower platen 150 mm diameter x 16 mm thick. Suitable for testing low-strength specimens.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Ball Seating for testing low strength cubes up to 100 mm

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Hand-operated Flexural Machine

[PRODUCT] 50 kN Mini-Flexural Machine (37-6040)
* Hand operated* Rugged, high strength frame* Double-action hydraulic pump* Dual calibrated (kN/lbf) gaugeThis compact flexural machine is designed for testing 100 mm and 150 mm square section beams. The base incorporates a series of bearer locating points, enabling a wide range of tests to be performed.The unit is self contained with hydraulic pressure applied through a double-action hand pump to a ram fitted in the top of the frame making this an ideal portable onsite quality control machine. A 200 mm diameter load gauge, dual calibrated to 50 kN x 0.1 kN and 11000 lbf x 50 lbf graduations is fitted as standard.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	50 kN Mini-Flexural Machine

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Accessories to connect ELE compression machines to the flexural/transverse frames

[PRODUCT] 100 kN Flexural Fitting Kit ADR Auto for 220 - 240 V AC, 50 Hz, 1 ph (37-6135/01)
These flexural frames can be used with a wide range of ELE compression machines. Simply select one of two fitting kits designed to link the flexural frame to either the ADR-Auto range of compression machines or any other ADR compression machine.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Flexural Fitting Kit for ADR Auto V2.0
	
Voltage Supply
	220-240 V 50 Hz

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/06)
Main: ADR-Auto V2.0 2000 BS Compression Machine (36-4150/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/01)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/06)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/01)
Main: ADR-Auto V2.0 3000 BS EN Compression Machine (36-4165/06)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/01)
Main: ADR-Auto V2.0 BS EN 2000/250kN Compression Machine (36-4155/06)
Main: ADR-Auto V2.0 BS EN 3000/250kN Compression Machine (36-4170/01)

[PRODUCT] 100 kN Flexural Fitting Kit ADR Auto for 110 - 120 V AC, 60 Hz, 1 ph (37-6135/02)
These flexural frames can be used with a wide range of ELE compression machines. Simply select one of two fitting kits designed to link the flexural frame to either the ADR-Auto range of compression machines or any other ADR compression machine.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Flexural Fitting Kit for ADR Auto V2.0
	
Voltage Supply
	110-120 V AC 60 Hz

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR-Auto V2.0 2000 Standard Compression Machine (36-4125/02)

[PRODUCT] 100kN Flexural Fitting Kit (ADR) Used for Connecting Flexural Frames to ADR Compression Machines. (37-6138)
These flexural frames can be used with a wide range of ELE compression machines. Simply select one of two fitting kits designed to link the flexural frame to either the ADR-Auto range of compression machines or any other ADR compression machine.

_Further Information_
**Not available for sale in the USA**

_Attributes_
Description
	Flexural Fitting Kit for ADR Touch

_Related Products_
Main: 100kN Flexural (Beams) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6130)
Main: 100kN Flexural and Transverse (Flags) Frame. Supplied Without Specimen Bearers and Fitting Kit. (37-6140)
Main: ADR Touch 1500 Compression Machine with Digital Readout. (36-0720/01)
Main: ADR Touch 2000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3280/01)
Main: ADR Touch 2000 Standard Compression Machine with Digital Readout. (36-3090/01)
Main: ADR Touch 3000 BS EN Compression Machine with Digital Readout and Self Centring Platens. (36-3320/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Voltage
	N/A for this Product Group