[DEPARTMENT] Cement

[CATEGORY] Chemical Tests
Chemical analysis plays an important part in the categorisation of cements and other construction materials such as lime. The use of analytical instrumentation such as flame photometry offers a simple and cost effective solution to the determination of the constituent parts of cement.

[PRODUCT GROUP] Loss-on-Ignition
The Loss-on-Ignition of Cement and Building Lime can be determined using a Muffle Furnace to oxidize the sample in air at 975 ± 25ºC.Muffle Furnace see Laboratory Equipment SectionCrucibles see Laboratory Equipment Section

[PRODUCT] Muffle Furnace (83-4170/01)

_Standards_
EN 196-2, EN 459-2, EN 13454-2, BS 1016-4, ISO 344, ISO 1171, ASTM D2361, ASTM D2795, ASTM D3714

_Attributes_
Description
	Muffle Furnace
	
Voltage Supply
	220 – 240 V AC, 50/60 Hz, 1 ph

_Specification_
External Dimensions (l x w x h)
	545 x 385 x 400 mm
	
Work chamber dimensions (l x w x h)
	300 x 200 x 120 mm
	
Internal volume
	6.9 litres
	
Maximum temperature
	1200 ºC
	
Electrical supply
	220 – 240 V AC, 50 - 60 Hz, 1 ph
	
Power supply
	3500 W
	
Weight
	130 kg

_Related Products_
Main: Heat of Hydration Apparatus (38-4600/06)
Main: Heat of Hydration Apparatus (38-4600/01)
Main: Rotatest 1500 (45-3810/01)
Main: Rotatest 3000 (45-3815/01)

[PRODUCT] Porcelain Crucible (82-3320)
30ml capacity complete with lid.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Porcelain Crucible
	
Capacity, ml
	30

_Related Products_
Main: Heat of Hydration Apparatus (38-4600/06)
Main: Heat of Hydration Apparatus (38-4600/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Flame Photometry
Today, cement is manufactured by a chemical process with raw materials being crushed, ground and blended before being heated in a rotary kiln until they combine chemically.

[PRODUCT GROUP] ELE Flame Photometer
The ELE Flame Photometer is built to a high specification and can be used with confidence for the most exacting analysis. It is a low temperature, single channel emission flame photometer with a large clear digital readout. The unit incorporates zero and gain controls with fine and coarse sensitivity, electronic ignition and automatic air supply regulation.The meter is supplied with sodium and potassium filters, fuel and air connections, nebuliser cleaning wire, hose connecting clips, auxiliary power plug, hexagon key, 2 lengths of drain tubing and a comprehensive instruction book and service manual. The unit is housed in a strong case.Special Note:The Flame Photometer requires a source of moisture-free air at 6 litres/minute at a pressure of 1 kg/cm². It also requires a fuel source for the flame and a regulator (see accessories).

[PRODUCT] ELE Flame Photometer (38-0200/01)
Special Note: The Flame Photometer requires a source of moisture-free air at 6 litres/minute at a pressure of 1 kg/cm². It also requires a fuel source for the flame and a regulator (see accessories).

_Standards_
EN 196-21, ASTM C114, TEST 17

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220-240 V AC, 50-60 Hz, 1 ph

_Attributes_
Description
	Flame Photometer
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Specification_
Dimensions (l x w x h)
	420 x 360 x 300 mm
	
Readout
	LED three 12.5 mm digits
	
Sensitivity Na  K  Ca
	3 to 100 ppm3 to 100 ppm5 to 100 ppm (optional filter)
	
Reproducibility
	1% CV for 20 consecutive samples using 10 ppm, set to read 100
	
Recorder Output
	Nominal 1.00 V for a reading of 100.0
	
Weight
	8 kg

_Related Products_
Accessory: Air Compressor (38-0320/01)
Accessory: Barium Filter (38-0260)
Accessory: Calcium Filter (38-0250)
Accessory: Regulators for Natural Gas (38-0270)
Accessory: Regulators for Propane Gas (38-0280)

[PRODUCT] Calcium Filter (38-0250)

_Standards_
EN 196-21, ASTM C114, TEST 17

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Calcium Filter

_Related Products_
Main: ELE Flame Photometer (38-0200/01)

[PRODUCT] Barium Filter (38-0260)

_Standards_
EN 196-21, ASTM C114, TEST 17

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Barium Filter

_Related Products_
Main: ELE Flame Photometer (38-0200/01)

[PRODUCT] Regulators for Natural Gas (38-0270)

_Standards_
EN 196-21, ASTM C114, TEST 17

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Natural Gas Regulator

_Related Products_
Main: ELE Flame Photometer (38-0200/01)

[PRODUCT] Regulators for Propane Gas (38-0280)

_Standards_
EN 196-21, ASTM C114, TEST 17

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Propane Gas Regulator

_Related Products_
Main: ELE Flame Photometer (38-0200/01)

[PRODUCT] Air Compressor (38-0320/01)
Supplies air at 6 litres/minute at a pressure of 1 kg/cm2, for use with 38-0200/01 Flame Photometer.

_Standards_
EN 196-21, ASTM C114, TEST 17

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Air Compressor
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Main: ELE Flame Photometer (38-0200/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Fineness
The fineness of cement is a property that must be carefully controlled during the manufacturing process. The total specific surface of the cement represents the surface area available for hydration. Various methods are in use to measure the specific surface of cements. For most purposes air permeability methods produce accurate, repeatable results.

[PRODUCT GROUP] Determination of Fineness Blaine Apparatus
This method has been adopted in Europe as the definitive means of determining the fineness of cement and other powder materials.The system is supplied complete with stainless steel cell, perforated disc and plunger, manometer U-tube, aspirator, bottle of manometer liquid and a box of filter papers.This method has been adopted in Europe as the definitive means of determining the fineness of cement and other powder materials.

[PRODUCT] Filter Papers (38-0650)
Accessory: 12.7mm diameter. Box of 100.

_Standards_
ASTM C204

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Filter Papers

_Related Products_
Main: Blaine Air Permeability Apparatus (38-1000)

[PRODUCT] Blaine Air Permeability Apparatus (38-1000)

_Standards_
EN 196-6, EN 459-2, EN 13286-44, BS 4359-2, ASTM C204, AASHTO T153

_Attributes_
Description
	Blaine Air Permeability Apparatus
	
Weight, lbs
	7

_Specification_
Cell
	Stainless steel; 12.70 ±0.10 mm i.d.
	
Disk
	0.9 ±0.1 mm thick with 30-40 one mm diam. holes.
	
Plunger
	Stainless steel.
	
Manometer
	U-tube glass with ground joint, stop cock and rubberbulb assembly.
	
Filter Paper
	12.70 mm diam.
	
Fluid
	Pure Mineral Oil.
	
Weight
	Net 7 lbs. (3.2 kg).

_Related Products_
Spare/Consumable: Blaine Air Permeability Cell (38-1000/15)
Accessory: Electronic Balance - 450 g x 0.001 g (78-5405/01)
Spare/Consumable: Filter Paper (38-0652)
Accessory: Filter Papers (38-0650)
Accessory: Manometer Liquid (38-0620)
Spare/Consumable: Manometer U-tube (38-1000/10)
Accessory: Reference Cement (38-0640)
Accessory: Timer Clock (81-0518)

[PRODUCT] Blaine Air Permeability Cell (38-1000/15)
Spare: Stainless steel with a perforated disc and plunger.

_Standards_
ASTM C204

_Attributes_
Description
	Blaine Air Permeability Cell

_Related Products_
Main: Blaine Air Permeability Apparatus (38-1000)

[PRODUCT] Manometer Liquid (38-0620)
Accessory: (Dibutylphthalate). 300ml bottle.

_Standards_
EN 196-21, ASTM C204

_Attributes_
Description
	Manometer Liquid

_Related Products_
Main: Blaine Air Permeability Apparatus (38-1000)

[PRODUCT] Manometer U-tube (38-1000/10)
Spare.

_Standards_
ASTM C204

_Attributes_
Description
	Manometer U-Tube

_Related Products_
Main: Blaine Air Permeability Apparatus (38-1000)

[PRODUCT] Reference Cement (38-0640)
Accessory: 10g sachet.

_Standards_
ASTM C204, AASHTO T153

_Attributes_
Description
	Reference Cement

_Related Products_
Main: Blaine Air Permeability Apparatus (38-1000)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Specific Gravity (relative density) of Hydration Cement
It is necessary to know the specific gravity of cement for various reasons related to its quality and use. In particular it will be necessary to determine the specific gravity as part of the determination of the specific surface of a cement. The ELE Le Chatelier Flask is a high specification unit that is individually calibrated and supplied with calibration certificate.

[PRODUCT] Le Chatelier Flask (38-1200)
For determining the density of hydraulic cement and lime, supplied complete with calibration certificate. Capacity 250ml. Graduated from 0 to 1ml and from 18 to 24ml graduations. Accurate to 0.05ml.

_Standards_
EN 196-6, ASTM C128, ASTM C188, E 694, AASHTO T133

_Attributes_
Description
	Le Chatelier Flask
	
Weight, oz.
	8

_Specification_
Graduations
	Zero mark represents 250 ml, the capacity of the large bulb; neck graduations from 0-1 ml in 0.1 ml divisions with two extra 0.1 ml graduations above the 1.0 and below the 0 marks; bulb portion of neck holds 17 ml; top portion of neck graduated from 18-24 ml in 0.1 ml divisions; 24 ml capacity.
	
Stopper
	Ground glass.
	
Weight
	Net 8 oz. (227 g).

_Related Products_
Accessory: Chattaway Spatula 125 mm (81-0180)
Accessory: Electronic Balance - 450 g x 0.001 g (78-5405/01)
Accessory: Water Bath - 12 litres (82-8500/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Consistency, Setting Time, Workability and Flow
Determination of setting time and soundness of cement requires the use of a neat cement paste of standard consistence. The Vicat method is usually specified as the test used to determine the water content which will produce the desired consistence.

[PRODUCT GROUP] Concrete Mortar Penetrometer
The Concrete Mortar Penetrometer is used for field and laboratory evaluations of the initial set of concrete mortars. The test involves inserting the penetrometer shaft to a depth of 25.4 mm at constant rate and time interval. The resistance in lbf/in² is shown on the penetrometer's direct-reading scale.

[PRODUCT] Pocket Concrete Penetrometer (38-2695)
Supplied complete with belt-loop, canvas carrying case.

_Standards_
ASTM C187, ASTM C191, ASTM C780

_Attributes_
Description
	Pocket Concrete Penetrometer
	
Dimensions, diam. X length, ”
	3/4” (19 mm) diam. x 7” (178 mm) long.

_Specification_
Dimensions
	19 x 178 mm (diameter x length)
	
Shaft Needle
	Steel, 1/20 inÂ² surface area
	
Range
	0 to 700 lbf/inÂ²
	
Scale
	Direct-reading, indicator sleeve holds reading until released
	
Weight
	227 g
	
Needle
	Steel shaft; 1/20 sq. in. surface area.
	
Range
	0 to 700 psi.
	
Scale
	Direct-reading; indicator sleeve holds reading until released.
	
Dimensions
	3/4â€ (19 mm) diam. x 7â€ (178 mm) long.
	
Carrying Case
	Canvas, with belt-loop.
	
Weight
	Net 8 oz. (227 g).

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Flow and Workability of Mortar Lime
To perform this test, a sample is placed on a metal surface which is then raised and dropped through a known height.

[PRODUCT] Flow Table (38-6000)
Manufactured from cast bronze as specified in BS and ASTM C230. Complete with Tripod and Baseplate.

_Standards_
BS 4551-1, BS 3892-1, ASTM C230

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Flow Table
	
Weight, kg
	25

_Related Products_
Accessory: ASTM Calipers (38-6080)
Accessory: Flow Mould (38-6040)
Accessory: Motorising Unit (38-6100/01)
Accessory: Plastic Tamper (38-6160)

[PRODUCT] Motorising Unit (38-6100/01)
For use with 38-6020. Operates the cam at a speed of 100 rpm. For 220-240V AC, 50 Hz, 1 ph.

_Standards_
ASTM C230

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Motorising Unit
	
Power Supply
	220 - 240 V AC, 50 Hz, 1 ph

_Related Products_
Accessory: ASTM Calipers (38-6080)
Accessory: Flow Mould (38-6040)
Main: Flow Table (38-6000)
Accessory: Plastic Tamper (38-6160)

[PRODUCT] Plastic Tamper (38-6160)

_Standards_
ASTM C230

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Plastic Tamper

_Related Products_
Accessory: ASTM Calipers (38-6080)
Accessory: Flow Mould (38-6040)
Main: Flow Table (38-6000)
Accessory: Motorising Unit (38-6100/01)

[PRODUCT] Flow Mould (38-6040)
Manufactured from bronze as specified in BS and ASTM.

_Standards_
ASTM C230

_Attributes_
Description
	Flow Mould

_Related Products_
Main: 10" Flow Table (38-6002)
Accessory: ASTM Calipers (38-6080)
Accessory: Flow Mould (38-6040)
Main: Flow Table (38-6000)
Accessory: Motorising Unit (38-6100/01)
Accessory: Plastic Tamper (38-6160)

[PRODUCT] ASTM Calipers (38-6080)
For measuring the diameter of the sample.

_Standards_
ASTM C230

_Attributes_
Description
	ASTM Calipers

_Related Products_
Main: 10" Flow Table (38-6002)
Accessory: Flow Mould (38-6040)
Main: Flow Table (38-6000)
Accessory: Motorising Unit (38-6100/01)
Accessory: Plastic Tamper (38-6160)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Setting Time
Determination of setting time and soundness of cement requires the use of a neat cement paste of standard consistence. The Vicat method is usually specified as the test used to determine the water content which will produce the desired consistence.

[PRODUCT GROUP] Vicat Method
This procedure is used to determine the quantity of water required to produce a cement paste of standard consistence.

[PRODUCT] Vicat Frame (38-2010)
Complete with consistency plunger, 10 mm diameter. Requires one initial or final set needle to make up test weight to 300g.

_Standards_
EN 196-3, EN 13454-2, ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Vicat Frame (less Needle Sets and Moulds)
	
Weight, kg
	1.3

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Accessory: Engineer's Steel Rule (81-0805)
Accessory: Harvard Trip Balance (78-7090)
Accessory: Timer Clock (81-0518)
Accessory: Vicat Mould (38-2200)
Accessory: Weights for Harvard Trip Balance (78-7110)

[PRODUCT] Consistency Plunger (38-2010/10)
Spare.

_Standards_
EN 196-3, EN 13454-2, ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Consistency Plunger

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Accessory: Engineer's Steel Rule (81-0805)
Accessory: Harvard Trip Balance (78-7090)
Accessory: Timer Clock (81-0518)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)
Accessory: Weights for Harvard Trip Balance (78-7110)

[PRODUCT] EN Initial and Final Set Needle (38-2110)
1.13mm diameter and 1.13mm diameter with special footing.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	EN Initial and Final Set Needle
	
Weight, kg
	0.018

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Vicat Mould (38-2300)
Accessory: Engineer's Steel Rule (81-0805)
Accessory: Harvard Trip Balance (78-7090)
Accessory: Timer Clock (81-0518)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)
Accessory: Weights for Harvard Trip Balance (78-7110)

[PRODUCT] Vicat Mould (38-2200)
Accessory: manufactured from brass and supplied complete with a ring and glass base plate.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Vicat Mould

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Main: Automatic Vicat Apparatus (38-2015/01)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Main: Vicat Frame (38-2010)

[PRODUCT] EN Vicat Mould (38-2300)
Accessory: manufactured from a hard rubber compound and supplied complete with a glass base plate.

_Standards_
EN 196-3

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	EN Vicat Mould

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Main: Automatic Vicat Apparatus (38-2015/01)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)

[PRODUCT] ASTM Vicat Mould (38-2660)
Accessory: manufactured from non-absorbent plastic and supplied complete with a glass base plate.

_Standards_
ASTM C187, ASTM C191

_Attributes_
Description
	ASTM Vicat Mould

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Main: Automatic Vicat Apparatus (38-2015/01)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Accessory: Engineer's Steel Rule (81-0805)
Accessory: Harvard Trip Balance (78-7090)
Accessory: Timer Clock (81-0518)
Main: Vicat Apparatus (38-2012)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)
Accessory: Weights for Harvard Trip Balance (78-7110)

[PRODUCT] ASTM Initial Set Needle (38-2620)
1 mm diameter.

_Standards_
ASTM C187, ASTM C191

_Attributes_
Description
	ASTM Initial Set Needle

_Related Products_
Accessory: ASTM Vicat Mould (38-2660)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Accessory: Engineer's Steel Rule (81-0805)
Accessory: Harvard Trip Balance (78-7090)
Accessory: Timer Clock (81-0518)
Main: Vicat Apparatus (38-2012)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)
Accessory: Weights for Harvard Trip Balance (78-7110)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Automatic Vicat
The Automatic Vicat Apparatus executes the test program using a fully automatic test cycle. The integral LCD display indicates test progress in real time. Firmware in the unit enables up to five user test profiles to be established. Integrated on-board memory will store up to 50 complete tests. On completion of the test the integral printer automatically prints all test data including a graph penetration with related data. As standard, the unit includes an RS232 serial port for connection to PC which, when used in conjunction with the supplied software, enables users to manage test data including graphing and report generation. The timed cycle of events is operator-selectable and penetrations can be selectable at intervals of 30 seconds, 1, 5, 15 or 30 minutes.

[PRODUCT] Needle Cleaning Device (38-2015/12)
Accessory.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Needle Cleaning Device

_Related Products_
Main: Automatic Vicat Apparatus (38-2015/01)

[PRODUCT] Printer Paper Rolls (38-2015/14)
Accessory: pack of 10.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Printer Paper Rolls

_Related Products_
Main: Automatic Vicat Apparatus (38-2015/01)

[PRODUCT] Mould Tank (38-2015/15)
Accessory: for testing samples under water as per EN 196-3, for use in temperature controlled laboratories.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Mould Tank

_Related Products_
Main: Automatic Vicat Apparatus (38-2015/01)

[PRODUCT] Consistency Plunger (38-2015/16)
Spare.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Consistency Plunger

_Related Products_
Main: Automatic Vicat Apparatus (38-2015/01)

[PRODUCT] EN Initial and Final Set Needle (38-2021)
Spare: 1.13mm diameter and 1.13mm diameter with special footing.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	EN Initial and Final Set Needle

_Related Products_
Main: Automatic Vicat Apparatus (38-2015/01)

[PRODUCT] ASTM Initial and Final Set Needle (38-2023)
Spare: 1mm x 2.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	ASTM Initial and Final Set Needle

_Related Products_
Main: Automatic Vicat Apparatus (38-2015/01)

[PRODUCT] Vicat Mould (38-2200)
Accessory: manufactured from brass and supplied complete with a ring and glass base plate.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Vicat Mould

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Main: Automatic Vicat Apparatus (38-2015/01)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Main: Vicat Frame (38-2010)

[PRODUCT] Automatic Vicat Apparatus (38-2015/01)
Complete with EN and ASTM Initial and Final needles, Consistency Plunger, Windows(R) software and RS232 cable, 1 x EN and ASTM Mould and Glass Plate. Suitable for continuous use in saturated humidity, at a controlled temperature of 20°C ± 1°C.

_Standards_
ASTM C187, ASTM C191

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220 - 240 V AC, 50 - 60 Hz, 1 ph.

_Attributes_
Description
	Automatic Vicat Apparatus (includes Needle Sets and Moulds for EN and ASTM)
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Spare/Consumable: ASTM Initial and Final Set Needle (38-2023)
Accessory: ASTM Vicat Mould (38-2660)
Spare/Consumable: Consistency Plunger (38-2015/16)
Spare/Consumable: EN Initial and Final Set Needle (38-2021)
Accessory: EN Vicat Mould (38-2300)
Accessory: Mould Tank (38-2015/15)
Accessory: Needle Cleaning Device (38-2015/12)
Accessory: Printer Paper Rolls (38-2015/14)
Accessory: Vicat Mould (38-2200)

[PRODUCT] EN Vicat Mould (38-2300)
Accessory: manufactured from a hard rubber compound and supplied complete with a glass base plate.

_Standards_
EN 196-3

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	EN Vicat Mould

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Accessory: ASTM Vicat Mould (38-2660)
Main: Automatic Vicat Apparatus (38-2015/01)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)

[PRODUCT] ASTM Vicat Mould (38-2660)
Accessory: manufactured from non-absorbent plastic and supplied complete with a glass base plate.

_Standards_
ASTM C187, ASTM C191

_Attributes_
Description
	ASTM Vicat Mould

_Related Products_
Accessory: ASTM Initial Set Needle (38-2620)
Main: Automatic Vicat Apparatus (38-2015/01)
Spare/Consumable: Consistency Plunger (38-2010/10)
Accessory: EN Initial and Final Set Needle (38-2110)
Accessory: EN Vicat Mould (38-2300)
Accessory: Engineer's Steel Rule (81-0805)
Accessory: Harvard Trip Balance (78-7090)
Accessory: Timer Clock (81-0518)
Main: Vicat Apparatus (38-2012)
Main: Vicat Frame (38-2010)
Accessory: Vicat Mould (38-2200)
Accessory: Weights for Harvard Trip Balance (78-7110)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Soundness
The soundness of cement and hydrated lime is of particular importance. It is essential that once hardened the paste does not undergo a large change in volume. The soundness of cements and limes can be determined by an expansion test using Le Chatelier Moulds. The method of curing lime differs from that of cements, lime being cured in a steam tank and cements in a water bath. The ASTM method uses a high-pressure steam vessel (Autoclave) to cure the specimens.

[PRODUCT GROUP] General Expansion of Dry Hydrated Lime by the Le Chatelier Method

[PRODUCT] Le Chatelier Mould (38-3005)
Comprising a split cylinder fitted with two indicator stems. The mould is supplied complete with two glass plates and a weight 100 g ±10 g. Three moulds required for each test.

_Standards_
BS 6463, EN 196-3, EN 459-2

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Le Chatelier Mould
	
Weight, kg
	0.9

_Related Products_
Accessory: Extensibility of Mould Apparatus BS (38-3200)
Accessory: Extensibility of Mould Apparatus EN (38-3205)
Accessory: Le Chatelier Water Bath (38-3420/01)
Accessory: Tamping Rod (38-3300)
Accessory: Trowel - Gauging (81-0335)

[PRODUCT] Extensibility of Mould Apparatus BS (38-3200)
Conforms to BS 6463. The unit comprises a metal sleeve with a hook and set screw to fit over one of the mould pointers, and a clamp to fit onto the other pointer of the mould. Supplied complete with one weight 100 g ±1 g.

_Standards_
EN 196-3

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Extensibility of Mould Apparatus BS
	
Weight, kg
	0.1

_Related Products_
Main: Le Chatelier Mould (38-3005)
Accessory: Le Chatelier Water Bath (38-3420/01)
Accessory: Tamping Rod (38-3300)
Accessory: Trowel - Gauging (81-0335)

[PRODUCT] Extensibility of Mould Apparatus EN (38-3205)
Conforms to EN196-3, 459-2. The unit comprises a metal sleeve with a hook and set screw to fit over one of the mould pointers, and a clamp to fit onto the other pointer of the mould. Supplied complete with one weight 300 g ±1 g.

_Standards_
EN 196-3

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Extensibility of Mould Apparatus EN
	
Weight, kg
	0.3

_Related Products_
Main: Le Chatelier Mould (38-3005)
Accessory: Tamping Rod (38-3300)

[PRODUCT] Tamping Rod (38-3300)
17 mm end diameter.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Tamping Rod
	
Weight, kg
	0.07

_Related Products_
Accessory: Extensibility of Mould Apparatus BS (38-3200)
Accessory: Extensibility of Mould Apparatus EN (38-3205)
Main: Le Chatelier Mould (38-3005)
Accessory: Le Chatelier Water Bath (38-3420/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Soundness of Cement Paste by the Le Chatelier Method

[PRODUCT] Le Chatelier Mould (38-3005)
Comprising a split cylinder fitted with two indicator stems. The mould is supplied complete with two glass plates and a weight 100 g ±10 g. Three moulds required for each test.

_Standards_
BS 6463, EN 196-3, EN 459-2

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Le Chatelier Mould
	
Weight, kg
	0.9

_Related Products_
Accessory: Extensibility of Mould Apparatus BS (38-3200)
Accessory: Extensibility of Mould Apparatus EN (38-3205)
Accessory: Le Chatelier Water Bath (38-3420/01)
Accessory: Tamping Rod (38-3300)
Accessory: Trowel - Gauging (81-0335)

[PRODUCT] Le Chatelier Water Bath (38-3420/01)
Manufactured from corrosion resistant material, complete with a removable rack to hold up to twelve moulds and timer unit.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Le Chatelier Water Bath
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Accessory: Extensibility of Mould Apparatus BS (38-3200)
Main: Le Chatelier Mould (38-3005)
Accessory: Tamping Rod (38-3300)
Accessory: Trowel - Gauging (81-0335)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Soundness of Portland Cement by the Autoclave Method
Specimens are cured in a high-pressure steam vessel and the change in specimen length is determined using Drying, Shrinkage and Moisture Movement Apparatus. The Autoclave provides high pressure steam curing of the specimens. The unit conforms to the requirements of ASTM. Supplied complete with safety valve, pressure gauge and thermostat controlled heater unit.Special Note:This unit draws a current of 20 amps.

[PRODUCT] Lid Sealing Gasket (38-3800/13)

_Standards_
ASTM C151

_Attributes_
Description
	Lid Sealing Gasket

_Related Products_
Main: Autoclave (38-3800/01)

[PRODUCT] Autoclave (38-3800/01)
The autoclave provides high pressure steam curing of the specimens and is supplied with a safety valve pressure gauge and controlled heater unit. The pressure vessel is independently certified and certificated. A specimen rack with capacity for 12 specimens included. The unit conforms to the requirements of ASTM C151. 220-240 V 50/60 Hz 1ph

_Standards_
ASTM C151

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Autoclave
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Spare/Consumable: Lid Sealing Gasket (38-3800/13)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Heat of Hydration Cement
The Heat of Hydration Apparatus is manufactured to the requirements specified in BS 4550. It comprises a Dewar flask, an internally lagged case, a constant speed electric stirrer, filler funnel and a Beckman-type thermometer complete with reader.

[PRODUCT] Dewar Flask (38-4600/10)
Spare.

_Standards_
BS 4550

_Attributes_
Description
	Dewar Flask

_Related Products_
Main: Heat of Hydration Apparatus (38-4600/01)
Main: Heat of Hydration Apparatus (38-4600/06)

[PRODUCT] Heat of Hydration Apparatus (38-4600/01)
For 220 - 240 V AC, 50 Hz, 1 ph.

_Standards_
BS 4550

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Heat of Hydration Apparatus
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Accessory: 200 mm Diameter Receiver (79-0020)
Accessory: 200mm Dia BS Sieve 125Mic Stainless Steel Mesh. (79-0110)
Accessory: 200mm Dia BS Sieve 600Mic Stainless Steel Mesh. (79-0200)
Spare/Consumable: Beckman Thermometer and Reader Glass (38-4600/12)
Accessory: Dessicator - Non-vacuum (82-2100)
Spare/Consumable: Dewar Flask (38-4600/10)
Accessory: Electronic Balance - 250 g x 0.1 mg (78-5335/01)
Spare/Consumable: Glass Paddle for Stirrer (38-4600/13)
Accessory: Harvard Trip Balance (78-7090)
Main: Mortar and Pestle Porcelain. (23-3505)
Main: Muffle Furnace (83-4170/01)
Main: Porcelain Crucible (82-3320)
Accessory: Sieve Brush Nylon (79-7210)
Accessory: Silica Gel (82-7091)
Accessory: Spatula 100 mm (81-0100)
Accessory: Timer Clock (81-0518)
Accessory: Weighing Bottle (82-1540)
Accessory: Weights for Harvard Trip Balance (78-7110)

[PRODUCT] Beckman Thermometer and Reader Glass (38-4600/12)
Spare: range 6ºC ± 0.01ºC

_Standards_
BS 4550

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Beckman Thermometer and Reader Glass

_Related Products_
Main: Heat of Hydration Apparatus (38-4600/06)
Main: Heat of Hydration Apparatus (38-4600/01)

[PRODUCT] Glass Paddle for Stirrer (38-4600/13)
Spare.

_Standards_
BS 4550

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Glass Paddle for Stirrer

_Related Products_
Main: Heat of Hydration Apparatus (38-4600/06)
Main: Heat of Hydration Apparatus (38-4600/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Air Content
Mortars are used for a variety of purposes, the most common being as a bond between brick and blockwork.

[PRODUCT GROUP] Air Content of Mortar, Masonry Cement and Lime by the Pressure Method
Both air content and density are important if durability and strength of mortar is to be adequate. Specifications often require minimum levels of air content and density. The equipment described enables standard tests to be performed on mortars and similar materials.

[PRODUCT] Air Entrainment Meter (38-7087)
0.75 litre capacity, complete with integral pump.

_Standards_
EN 413-2, BS 459-2

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Capacity litres
	0.75
	
Description
	Air Entrainment Meter

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Fly Ash
Fly Ash of Pulverised Fuel Ash is a by-product of coal-fired power stations. It is a fine material with spherical particles. Uses include as an additive in composite cements, as a cementitious component in concrete and as a filler in certain types of asphalt. Various test methods are specified in BS and EN Standards and include the determination of moisture content, water requirement, strength, loss-on-ignition, initial setting time, and soundness. These tests are based on those described in BS EN196. A major requirement for Fly Ash is consistency of fineness.

[PRODUCT GROUP] Loss-on-Ignition
This method is for cement specified in EN196-2 with an ignition time of 1 hour at 975ºC.

[PRODUCT] Muffle Furnace (83-4170/01)

_Standards_
EN 196-2, EN 459-2, EN 13454-2, BS 1016-4, ISO 344, ISO 1171, ASTM D2361, ASTM D2795, ASTM D3714

_Attributes_
Description
	Muffle Furnace
	
Voltage Supply
	220 – 240 V AC, 50/60 Hz, 1 ph

_Specification_
External Dimensions (l x w x h)
	545 x 385 x 400 mm
	
Work chamber dimensions (l x w x h)
	300 x 200 x 120 mm
	
Internal volume
	6.9 litres
	
Maximum temperature
	1200 ºC
	
Electrical supply
	220 – 240 V AC, 50 - 60 Hz, 1 ph
	
Power supply
	3500 W
	
Weight
	130 kg

_Related Products_
Main: Heat of Hydration Apparatus (38-4600/06)
Main: Heat of Hydration Apparatus (38-4600/01)
Main: Rotatest 1500 (45-3810/01)
Main: Rotatest 3000 (45-3815/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Activity Index
The activity index is the ratio (in percent) of the compressive strength of standard mortar prisms 40 x 40 x 160 mm, prepared with 75% reference cement and 25% fly ash, to standard mortar prisms prepared with reference cement alone. The equipment required comprises that used to prepare specimens and determine their compressive strength in accordance with EN196-1.

[PRODUCT] ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/01)
* 250 kN maximum capacity* Calibration accuracy to BS EN ISO 7500-1; ASTM E4* Automatic loading cycle* 25 kN low capacity frame supplied as standard* Tests a wide variety of specimen sizes* Tests mortar, lime, cement and Fly Ash* Complete with compression/flexural jigs and platen sets* Supplied with Windows(R) download software as standardThe ADR-Auto 250/25 Machine provides consistent automatic testing of a wide range of specimens. The machine comprises a standard ELE 250/25 kN load frame and ADR-Auto console and incorporates all the features included in the ADR-Auto series concrete testing machines.As standard the machine is supplied with platens fitted to the load frame, compression jig with 40 mm and 50mm/2 inch square platen sets and flexural jig for testing 40.1 x 40 x 160 mm prisms. The availability of the 25 kN low capacity load frame as standard extends the test capability of the machine for low strength compression or flexural testing. The automatic loading cycle is controlled by a closedloop microprocessor hydraulic system incorporated with the display in the ADR-Auto console attached to the load frame. A serial output port is built into the system, enabling test data to be stored in memory (up to 500 test results) for subsequent downloading to PC or suitable printer.

_Standards_
EN 196-1, EN 459-2, EN 1744, EN 1015-11, EN 13454-2, BS 3892-1, BS 4551-1, ASTM C109

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220 - 240 V AC, 50 Hz, 1 ph.

_Attributes_
Voltage Supply
	220 – 240 V AC 50 Hz
	
Description
	ADR-Auto V2.0 250/25 Cement Machine

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
Accessory: Printer (39-4859/01)
Accessory: Set of Distance Pieces (39-6220)

[PRODUCT] ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
* 250 kN maximum capacity* Calibration accuracy to BS EN ISO 7500-1; ASTM E4* Automatic loading cycle* 25 kN low capacity frame supplied as standard* Tests a wide variety of specimen sizes* Tests mortar, lime, cement and Fly Ash* Complete with compression/flexural jigs and platen sets* Supplied with Windows(R) download software as standardThe ADR-Auto 250/25 Machine provides consistent automatic testing of a wide range of specimens. The machine comprises a standard ELE 250/25 kN load frame and ADR-Auto console and incorporates all the features included in the ADR-Auto series concrete testing machines.As standard the machine is supplied with platens fitted to the load frame, compression jig with 40 mm and 50mm/2 inch square platen sets and flexural jig for testing 40.1 x 40 x 160 mm prisms. The availability of the 25 kN low capacity load frame as standard extends the test capability of the machine for low strength compression or flexural testing. The automatic loading cycle is controlled by a closedloop microprocessor hydraulic system incorporated with the display in the ADR-Auto console attached to the load frame. A serial output port is built into the system, enabling test data to be stored in memory (up to 500 test results) for subsequent downloading to PC or suitable printer.

_Standards_
EN 196-1, EN 459-2, EN 1744, EN 1015-11, EN 13454-2, BS 3892-1, BS 4551-1, ASTM C109

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220-240 V AC, 60 Hz, 1 ph.

_Attributes_
Voltage Supply
	220 - 240 V AC 60 Hz
	
Description
	ADR-Auto V2.0 250/25 Cement Machine

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/01)
Accessory: Printer (39-4859/01)
Accessory: Set of Distance Pieces (39-6220)
Accessory: Three-gang Mould (39-1100)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Soundness

[PRODUCT] Le Chatelier Mould (38-3005)
Comprising a split cylinder fitted with two indicator stems. The mould is supplied complete with two glass plates and a weight 100 g ±10 g. Three moulds required for each test.

_Standards_
BS 6463, EN 196-3, EN 459-2

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Le Chatelier Mould
	
Weight, kg
	0.9

_Related Products_
Accessory: Extensibility of Mould Apparatus BS (38-3200)
Accessory: Extensibility of Mould Apparatus EN (38-3205)
Accessory: Le Chatelier Water Bath (38-3420/01)
Accessory: Tamping Rod (38-3300)
Accessory: Trowel - Gauging (81-0335)

[PRODUCT] Le Chatelier Water Bath (38-3420/01)
Manufactured from corrosion resistant material, complete with a removable rack to hold up to twelve moulds and timer unit.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Le Chatelier Water Bath
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Related Products_
Accessory: Extensibility of Mould Apparatus BS (38-3200)
Main: Le Chatelier Mould (38-3005)
Accessory: Tamping Rod (38-3300)
Accessory: Trowel - Gauging (81-0335)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Fineness of Fly Ash (Wet Sieving)

[PRODUCT] Spray Nozzle Apparatus (38-7600)
Comprising a spray nozzle 17.5 mm ID with 17 holes as specified in EN451, a vacuum pressure gauge, 160 kPa graduated at 5 kPa divisions and fittings to attach the apparatus to a standard domestic water supply. Supplied without sieve.

_Standards_
BS 3892-1, EN 451-2, ASTM C430

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Spray Nozzle Apparatus
	
Weight, kg
	2.1

_Related Products_
Accessory: 45 μm Sieve (38-7600/12)

[PRODUCT] 45 μm Sieve (38-7600/12)
Stainless steel mesh, 50 mm internal diameter.

_Standards_
BS 3892-1, EN 451-2, ASTM C430

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	45 μm Sieve

_Related Products_
Main: Spray Nozzle Apparatus (38-7600)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Mixing, Moulding, Curing and Strength

[CATEGORY] Mixing
The correct mixing sequence and homogenity of mix is important if consistent, repeatable test results are to be obtained. Mixers should be powerful enough to ensure that the motor's speed is not affected by the mix constituents and designed to ensure that the mixer action and blade does not break down individual sand particles and preferably provide automatic mixing cycles. In the USA, ASTM C109 and C190 are the definitive methods for determining compressive and tensile strength. The BS 4550 method using either 70.7 mm or 100 mm cubes has been retained in the UK only for comparative purposes. EN196-1 is now the definitivemethod. 

[PRODUCT GROUP] Automatic/Manual 5 Litre Nominal Capacity Mortar Mixer

[PRODUCT] Automatic/Manual 5 litre nominal capacity Mortar Mixer (39-0035/01)
* New Microprocessor control* New mix program selector* Complies with latest EN Standards update* Choice of automatic mixing cycles* Sand and water dispenser supplied as standardThis mixer is designed to mix mortars and cement pastes to the requirements of the above Standards. The mixing paddle has a planetary motion and is driven by a motor with a microprocessor based speed and program controller. The mixer can be operated either in an automatic or manual mode. When the mixer is used in the manual mode, the two mixing speeds can be changed by means of a rocker switch, without switching off the motor. In the automatic mode any one of the preset mixing programs may be selected.

_Standards_
EN 196-1, EN 196-3, EN 413-2, EN 459-2, EN 1744-1, EN 13279-2, EN 1015-2, EN 13395-1, EN 13454-2, ISO 679, BS 3892-1, BS 3892-3, BS 6463-103, BS 4551-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** Complete with bowl and paddle, sand and Water dispensers. For 220 - 240 V AC, 50 - 60 Hz, 1 ph.

_Attributes_
Description
	Automatic/Manual Mortar Mixer
	
Power Supply
	220 - 240 V AC, 50 - 60 Hz, 1 ph

_Specification_
Dimensions (l x w x h)
	530 x 350 x 580 mm
	
Speeds (rpm) Low, High
	Paddle: 140 ± 5, 285 ± 10Mixing Head: 62 ± 5, 125 ± 10
	
Rated Power
	180 W
	
Bowl Capacity
	5 litres approx.
	
Weight
	54 kg

_Related Products_
Spare/Consumable: Bowl (39-0031/11)
Accessory: Bowl Cover (39-0060)
Spare/Consumable: Paddle (39-0031/10)
Accessory: Scraper (39-0065)

[PRODUCT] Paddle (39-0031/10)
Stainless steel complies with EN196.

_Standards_
BS 3892-1, EN 451-2

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Paddle

_Related Products_
Main: Automatic/Manual 5 litre nominal capacity Mortar Mixer (39-0035/01)

[PRODUCT] Bowl (39-0031/11)
Stainless steel complies with EN196. 5 litre capacity (approx).

_Standards_
BS 3892-1, EN 451-2

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Bowl

_Related Products_
Main: Automatic/Manual 5 litre nominal capacity Mortar Mixer (39-0035/01)

[PRODUCT] Bowl Cover (39-0060)

_Standards_
EN 196-1, EN 196-3, EN 413-2, EN 459-2, EN 1744-1, EN 13279-2, EN 1015-2, EN 13395-1, EN 13454-2, ISO 679, BS 3892-1, BS 3892-3, BS 6463-103, BS 4551-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Bowl Cover

_Related Products_
Main: Automatic/Manual 5 litre nominal capacity Mortar Mixer (39-0035/01)

[PRODUCT] Scraper (39-0065)
Plastic 200mm long. Pack of 5.

_Standards_
EN 196-1, EN 196-3, EN 413-2, EN 459-2, EN 1744-1, EN 13279-2, EN 1015-2, EN 13395-1, EN 13454-2, ISO 679, BS 3892-1, BS 3892-3, BS 6463-103, BS 4551-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Scraper

_Related Products_
Main: Automatic/Manual 5 litre nominal capacity Mortar Mixer (39-0035/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Moulding
The successful preparation and moulding of prisms, cubes and briquettes is essential if subsequent strength tests on the specimens are to be meaningful. Moulds should be manufactured from material which is capable of retaining its form under heavy usage. The equipment detailed in this section has been designed and manufactured to meet the requirements for moulding laid down in the various standards.

[PRODUCT GROUP] Moulding of Prisms
Two methods of moulding and compaction are used in the various testing standards. The jolting table method is usually described as the reference method and a vibratory method is permitted as an alternative.

[PRODUCT] Feeding Hopper (39-1120)
For 39-1100 Mould.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Feeding Hopper

_Related Products_
Main: Jolting Table 220 - 240 V 50 Hz (39-1150/01)
Main: Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)
Accessory: Three-gang Mould (39-1100)

[PRODUCT] Three-gang Mould (39-1100)
For 40.1 x 40 x 160 mm mortar prisms. This mould is manufactured to a very high specification. Supplied with glass plate.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Three-gang Mould
	
Weight, kg
	12.2

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
Accessory: Feeding Hopper (39-1120)
Spare/Consumable: Glass Plate (39-1100/10)
Main: Jolting Table 220 - 240 V 50 Hz (39-1150/01)
Main: Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)
Spare/Consumable: Mortar Sand (39-1170)

[PRODUCT] Glass Plate. (24-0430)
500 mm square x 10 mm thick.

_Standards_
BS 1377, EN 1997-2

_Attributes_
Description
	Glass plate
	
BS/EN Standard
	Yes

_Related Products_
Main: Bulk Density Measure 10 Litre (34-2830)
Main: Liquid Limit Device BS with Counter. C/W Metal Grooving Tool & Test Gauge. (24-0410)
Main: Motorised Liquid Limit Device W/ Counter BS 220-240V 50Hz 1Ph. (24-0417/01)

[PRODUCT] Scraper (39-1130)
Double-ended, used for spreading and levelling mortar in mould.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Scraper

_Related Products_
Main: Jolting Table 220 - 240 V 50 Hz (39-1150/01)
Main: Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)

[PRODUCT] Mortar Sand (39-1170)
Graded pack for 3 prisms. 1350g pack.

_Standards_
EN 196-1, EN 413-2, EN 459-2, EN 1744-1, EN 1015-10, EN 1015-11, EN 13454-2, ISO 679, BS 3892-1, BS 4551-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Mortar Sand

_Related Products_
Main: Jolting Table 220 - 240 V 50 Hz (39-1150/01)
Main: Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)
Accessory: Three-gang Mould (39-1100)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Jolting Table
This machine consists of a mould table seated on a rotating cam driven at 60 revolutions per minute. The apparatus is supplied with a remote mains switch box, incorporating a push button start/stop control, and automatic stop control at end of test.

[PRODUCT] Jolting Table 220 - 240 V 50 Hz (39-1150/01)
Supplied without moulds.

_Standards_
EN 196-1, EN 413-2, EN 459-2, EN 1744-1, EN 1015-10, EN 1015-11, EN 13454-2, ISO 679, BS 3892-1, BS 4551-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Voltage Supply
	220 - 240 V AC 50 Hz
	
Description
	Jolting Table

_Related Products_
Accessory: Feeding Hopper (39-1120)
Main: Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)
Spare/Consumable: Mortar Sand (39-1170)
Spare/Consumable: Scraper (39-1130)
Accessory: Three-gang Mould (39-1100)

[PRODUCT] Jolting Table 220 - 240 V AC 60 Hz (39-1150/06)
Supplied without moulds.

_Standards_
EN 196-1, EN 413-2, EN 459-2, EN 1744-1, EN 1015-10, EN 1015-11, EN 13454-2, ISO 679, BS 3892-1, BS 4551-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Voltage Supply
	220 - 240 V AC 60 Hz
	
Description
	Jolting Table

_Related Products_
Accessory: Feeding Hopper (39-1120)
Main: Jolting Table 220 - 240 V 50 Hz (39-1150/01)
Main: Large Curing Tank C/W with Circulating Pump Heater/Thermostat Unit and Lower Rack (34-6575/01)
Spare/Consumable: Mortar Sand (39-1170)
Spare/Consumable: Scraper (39-1130)
Accessory: Three-gang Mould (39-1100)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Voltage
	N/A for this Product Group

[PRODUCT GROUP] Moulding of 50 mm and 100 mm Specimens

[PRODUCT] Three-gang Mould (39-0410)
For 50mm mortar cubes. Manufactured from cast iron with simple cube release mechanism.

_Standards_
BS 1881-131, ASTM C109

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Three-gang Mould
	
Weight, kg
	6.5

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Moulding of 70.7 mm Mortar Cubes

[PRODUCT] Cube Mould (39-0100)
Manufactured from steel to dimensions specified in the relevant British Standard. Supplied complete with baseplate. Three moulds required for each test.

_Standards_
BS 4550

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Cube Mould
	
Weight, kg
	2.9

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] Moulding of Mortar Briquettes

[PRODUCT] Briquette Mould (39-1000)
Manufactured to the dimensions in the relevant specification. Two part construction, supplied complete with baseplate.

_Standards_
ASTM C307

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Briquette Mould
	
Weight, kg
	1.3

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[CATEGORY] Curing
Prior to testing, EN 196 requires prisms to be cured for a period of at least 24 hours at 20 ±1°C, 90% RH minimum. The prisms are then demoulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days.

[PRODUCT GROUP] Humidity Cabinet ASTM
Prior to testing, ASTM C109 requires prisms to be cured for a period of at least 24 hours at 23ºC ±2ºC, 95 % RH minimum. The prisms are then de-moulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days.

[PRODUCT] Humidity Cabinet ASTM 150 Litre Capacity (SP39-1401/01)
 	* Complete with temperature and humidity chart recorder 	* Micro-processer controller for temperature and humidity for precise and reliable control 	* Stainless Steel interior with adjustable shelves 	* CFC-free polyurethane insulation to provide efficient thermal stability 	* 12mm access portPrior to testing, ASTM C109 requires prisms to be cured for a period of at least 24 hours at 23ºC ±2ºC, 95 % RH minimum. The prisms are then de-moulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days. The Humidity Cabinet is built to a high specification and is designed for the early curing of mortar prisms prior to storing under water. Relative humidity up to 98%.

_Further Information_
for 220-240 V AC 50 Hz 1ph

_Attributes_
Voltage Supply
	220 - 240 V AC 50 Hz 1ph
	
Description
	Humidity Cabinet
	
Capacity, litres
	150

_Specification_
Temperature Range
	+5 °C to 60 °C
	
Temperature Control
	0.2 °C at 20°C
	
Temperature Variation
	± 0.5 °C at 20°C
	
Humidity Range
	0ï½ž98%
	
External Dimensions (mm)
	1075 × 635 × 660
	
Internal Dimensions (mm)
	590 × 510 × 490
	
Shelves
	4 - Holds 6 x 39-1100 moulds
	
Shelf Capacity
	15kg
	
Input Power
	800 Watt
	
Weight
	100 kg

[PRODUCT] Humidity Cabinet ASTM 150 Litre Capacity (SP39-1401/06)
 	* Complete with temperature and humidity chart recorder 	* Micro-processer controller for temperature and humidity for precise and reliable control 	* Stainless Steel interior with adjustable shelves 	* CFC-free polyurethane insulation to provide efficient thermal stability 	* 12mm access portPrior to testing, ASTM C109 requires prisms to be cured for a period of at least 24 hours at 23ºC ±2ºC, 95 % RH minimum. The prisms are then de-moulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days. The Humidity Cabinet is built to a high specification and is designed for the early curing of mortar prisms prior to storing under water. Relative humidity up to 98%.

_Further Information_
for 220-240 V AC 60 Hz 1ph

_Attributes_
Voltage Supply
	220 - 240 V AC 60 Hz 1ph
	
Description
	Humidity Cabinet
	
Capacity, litres
	150

_Specification_
Temperature Range
	+5 °C to 60 °C
	
Temperature Control
	0.2 °C at 20°C
	
Temperature Variation
	± 0.5 °C at 20°C
	
Humidity Range
	0ï½ž98%
	
External Dimensions (mm)
	1075 × 635 × 660
	
Internal Dimensions (mm)
	590 × 510 × 490
	
Shelves
	4 - Holds 6 x 39-1100 moulds
	
Shelf Capacity
	15kg
	
Input Power
	800 Watt
	
Weight
	100 kg

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Capacity, litres
	Voltage
	N/A for this Product Group

[PRODUCT GROUP] Humidity Cabinet BS EN
Prior to testing, EN 196 requires prisms to be cured for a period of at least 24 hours at 20 ±1ºC, 90 % RH minimum. The prisms are then de-moulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days.

[PRODUCT] Humidity Cabinet BS EN 150 Litre Capacity 50Hz (SP39-1400/01)
 	* Micro-processer controller for temperature and humidity for precise and reliable control 	* Stainless Steel interior with adjustable shelves 	* CFC-free polyurethane insulation to provide efficient thermal stability 	* 12mm access portPrior to testing, EN 196 requires prisms to be cured for a period of at least 24 hours at 20 ±1ºC, 90 % RH minimum. The prisms are then de-moulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days. The Humidity Cabinet is built to a high specification and is designed for the early curing of mortar prisms prior to storing under water. Relative humidity up to 98%.

_Attributes_
Description
	Humidity Cabinet
	
Capacity, litres
	150
	
Voltage Supply
	220 - 240 V AC 50 Hz 1ph
	
Power Supply
	220-240 V AC 50 Hz 1ph

_Specification_
Temperature Range
	+5 °C to 60 °C
	
Temperature Control
	0.2 °C at 20°C
	
Temperature Variation
	± 0.5 °C at 20°C
	
Humidity Range
	0ï½ž98%
	
External Dimensions (mm)
	1075 × 635 × 660 
	
Internal Dimensions (mm)
	590 × 510 × 490
	
Shelves
	4 Holds 6 x 39-1100 moulds
	
Shelf Capacity
	15 kg
	
Input Power
	800 Watt
	
Weight
	195 kg

_Related Products_
Main: Humidity Cabinet BS EN 150 Litre Capacity 60Hz (SP39-1400/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/01)
Spare/Consumable: Replacement Circular Charts (39-1300/10)

[PRODUCT] Humidity Cabinet BS EN 150 Litre Capacity 60Hz (SP39-1400/06)
 	* Micro-processer controller for temperature and humidity for precise and reliable control 	* Stainless Steel interior with adjustable shelves 	* CFC-free polyurethane insulation to provide efficient thermal stability 	* 12mm access portPrior to testing, EN 196 requires prisms to be cured for a period of at least 24 hours at 20 ±1ºC, 90 % RH minimum. The prisms are then de-moulded and stored under water for the required curing time, usually 48 hours, 72 hours, 7 and 28 days. The Humidity Cabinet is built to a high specification and is designed for the early curing of mortar prisms prior to storing under water. Relative humidity up to 98%.

_Attributes_
Description
	Humidity Cabinet
	
Capacity, litres
	150
	
Voltage Supply
	220 - 240 V AC 60 Hz 1ph
	
Capacity, g
	150 l
	
Power Supply
	220-240 V AC 60 Hz 1ph

_Specification_
Temperature Range
	+5 °C to 60 °C
	
Temperature Control
	0.2 °C at 20°C
	
Temperature Variation
	± 0.5 °C at 20°C
	
Humidity Range
	0ï½ž98%
	
External Dimensions (mm)
	1075 × 635 × 660 
	
Internal Dimensions (mm)
	590 × 510 × 490
	
Shelves
	4 Holds 6 x 39-1100 moulds
	
Shelf Capacity
	15 kg
	
Input Power
	800 Watt
	
Weight
	195 kg

_Related Products_
Main: Humidity Cabinet BS EN 150 Litre Capacity 50Hz (SP39-1400/01)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/01)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/06)
Spare/Consumable: Replacement Circular Charts (39-1300/10)

[PRODUCT] Humidity Cabinet to En196 320 Litre Capacity (39-1300/01)
For 220 - 240 V AC, 50 Hz, 1 ph.

_Standards_
EN 196-1, EN 459-2, BS 3892-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** 10 Reinforced Shelves and Circular Chart Recorder

_Attributes_
Description
	Humidity Cabinet
	
Capacity, litres
	320
	
Voltage Supply
	220 - 240 V AC, 50 Hz, 1 ph
	
Power Supply
	220-240 V AC, 50 Hz, 1 ph

_Specification_
Capacity
	320 litres
	
Dimensions External, Internal
	660 x 635 x 1745 mm,490 x 510 x 1275 mm
	
Temperature Range
	+5.0°C to +60°C
	
Fluctuation (better than)
	± 0.2ºC
	
Variation (better than)
	± 0.5ºC
	
Recorder:Circular chart type,Temperature,Humidity
	7 day,0 – 50ºC,0 – 100% RH
	
Rated power
	850 Watt
	
Number of shelves
	10
	
Weight
	151 kg

_Related Products_
Main: Humidity Cabinet BS EN 150 Litre Capacity 50Hz (SP39-1400/01)
Main: Humidity Cabinet BS EN 150 Litre Capacity 60Hz (SP39-1400/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/06)
Spare/Consumable: Replacement Circular Charts (39-1300/10)

[PRODUCT] Humidity Cabinet to En196 320 Litre Capacity (39-1300/06)
For 220 - 240 V AC, 60 Hz, 1 ph.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** 10 Reinforced Shelves and Circular Chart Recorder

_Attributes_
Description
	Humidity Cabinet
	
Capacity, litres
	320
	
Voltage Supply
	220 - 240 V AC, 60 Hz, 1 ph
	
Power Supply
	220-240 V AC, 60 Hz, 1 ph

_Related Products_
Main: Humidity Cabinet BS EN 150 Litre Capacity 50Hz (SP39-1400/01)
Main: Humidity Cabinet BS EN 150 Litre Capacity 60Hz (SP39-1400/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/01)
Spare/Consumable: Replacement Circular Charts (39-1300/10)

[PRODUCT] Replacement Circular Charts (39-1300/10)

_Standards_
EN 196-1, EN 459-2, BS 3892-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Circular Charts

_Related Products_
Main: Humidity Cabinet BS EN 150 Litre Capacity 50Hz (SP39-1400/01)
Main: Humidity Cabinet BS EN 150 Litre Capacity 60Hz (SP39-1400/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/06)
Main: Humidity Cabinet to En196 320 Litre Capacity (39-1300/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Capacity, litres
	Voltage
	N/A for this Product Group

[CATEGORY] Strength

[PRODUCT GROUP] 10 kN Flexural/ Tensile Testing Machine

[PRODUCT] 10kN Flexural/Tensile Testing Machine (39-7100/01)
This single lever machine is designed for flexural tests on 40.1 x 40 x 160 mm mortar prisms and tensile tests on mortar briquettes. The rate of applied loading for flexural testing is to EN196-1. Load is applied by a weight travelling along the beam at a constant rate, driven by a motor/gearbox. Readings are made by means of a cursor visible through a window in the moving weight. Failure of a specimen triggers a switch mechanism and brings the weight to a halt immediately. To prevent overloading, a sensor is incorporated in the weight and automatically stops the machine at its maximum capacity of 10 kN. Supplied complete with flexural and tensile jaws.

_Standards_
EN 196-1

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220 - 240 V AC, 50 Hz, 1 ph.

_Attributes_
Description
	10 kN Flexural/Tensile Testing Machine
	
Power Supply
	220 - 240 V AC, 50 Hz, 1 ph

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	N/A for this Product Group

[PRODUCT GROUP] ADR-Auto V2.0 250/25 Compression Machine

[PRODUCT] ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/01)
* 250 kN maximum capacity* Calibration accuracy to BS EN ISO 7500-1; ASTM E4* Automatic loading cycle* 25 kN low capacity frame supplied as standard* Tests a wide variety of specimen sizes* Tests mortar, lime, cement and Fly Ash* Complete with compression/flexural jigs and platen sets* Supplied with Windows(R) download software as standardThe ADR-Auto 250/25 Machine provides consistent automatic testing of a wide range of specimens. The machine comprises a standard ELE 250/25 kN load frame and ADR-Auto console and incorporates all the features included in the ADR-Auto series concrete testing machines.As standard the machine is supplied with platens fitted to the load frame, compression jig with 40 mm and 50mm/2 inch square platen sets and flexural jig for testing 40.1 x 40 x 160 mm prisms. The availability of the 25 kN low capacity load frame as standard extends the test capability of the machine for low strength compression or flexural testing. The automatic loading cycle is controlled by a closedloop microprocessor hydraulic system incorporated with the display in the ADR-Auto console attached to the load frame. A serial output port is built into the system, enabling test data to be stored in memory (up to 500 test results) for subsequent downloading to PC or suitable printer.

_Standards_
EN 196-1, EN 459-2, EN 1744, EN 1015-11, EN 13454-2, BS 3892-1, BS 4551-1, ASTM C109

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220 - 240 V AC, 50 Hz, 1 ph.

_Attributes_
Voltage Supply
	220 – 240 V AC 50 Hz
	
Description
	ADR-Auto V2.0 250/25 Cement Machine

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
Accessory: Printer (39-4859/01)
Accessory: Set of Distance Pieces (39-6220)

[PRODUCT] ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
* 250 kN maximum capacity* Calibration accuracy to BS EN ISO 7500-1; ASTM E4* Automatic loading cycle* 25 kN low capacity frame supplied as standard* Tests a wide variety of specimen sizes* Tests mortar, lime, cement and Fly Ash* Complete with compression/flexural jigs and platen sets* Supplied with Windows(R) download software as standardThe ADR-Auto 250/25 Machine provides consistent automatic testing of a wide range of specimens. The machine comprises a standard ELE 250/25 kN load frame and ADR-Auto console and incorporates all the features included in the ADR-Auto series concrete testing machines.As standard the machine is supplied with platens fitted to the load frame, compression jig with 40 mm and 50mm/2 inch square platen sets and flexural jig for testing 40.1 x 40 x 160 mm prisms. The availability of the 25 kN low capacity load frame as standard extends the test capability of the machine for low strength compression or flexural testing. The automatic loading cycle is controlled by a closedloop microprocessor hydraulic system incorporated with the display in the ADR-Auto console attached to the load frame. A serial output port is built into the system, enabling test data to be stored in memory (up to 500 test results) for subsequent downloading to PC or suitable printer.

_Standards_
EN 196-1, EN 459-2, EN 1744, EN 1015-11, EN 13454-2, BS 3892-1, BS 4551-1, ASTM C109

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA** For 220-240 V AC, 60 Hz, 1 ph.

_Attributes_
Voltage Supply
	220 - 240 V AC 60 Hz
	
Description
	ADR-Auto V2.0 250/25 Cement Machine

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/01)
Accessory: Printer (39-4859/01)
Accessory: Set of Distance Pieces (39-6220)
Accessory: Three-gang Mould (39-1100)

[PRODUCT] Set of Distance Pieces (39-6220)
Accessory: for testing samples 40mm, 50mm, 70.7mm and 100mm. Note: These items are required when testing above sample sizes NOT using the compression jig.

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Set of Distance Pieces

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/01)

[PRODUCT] Printer (39-4859/01)
Accessory

_Further Information_
**NOT AVAILABLE FOR SALE IN THE USA**

_Attributes_
Description
	Printer

_Related Products_
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/06)
Main: ADR-Auto V2.0 250/25 Cement Machine C/W Compression and Flexural Jigs and Platen Sets (39-6160/01)

[GROUPED PRODUCT MATRIX]
Model No.
	Desc
	Voltage
	N/A for this Product Group